Electromagnetic Exploration of Historical Oil Paintings – possible application venues and preliminary results

Beatrice G. Boracchi1,2, Francisco Mederos-Henry2,3, Isabelle Huynen1

1 ELEN-ICTEAM, Universitee Catholique de Louvain, Louvain-La-Neuve, Belgium

2 Materials Science for Conservation Research unit, Laboratories Department, Royal Institute for Cultural Heritage (KIK-IRPA), Bruxelles, Belgium

3 Research Centre in Archaeology and Heritage, Université Libre de Bruxelles (ULB), Brussels, Belgium

The study of the properties of siccative oils has been central for the understanding of the degradation processes that affects oil paintings. Considerable attention has been given to the chemical characterization of different oil systems representative of oils used for painting through the ages, since its development in the XV century by the Flemish primitives. Nonetheless, the study of their dielectric properties remains unexplored. The study of such fundamental properties of oil binders constitutes thus a new approach to understanding their behavior and to offer a conceptual framework explaining some of the ionic-driven processes observed in historical oil paintings, from paint film formation to their degradation. In our work, attention has been given to the interaction between oil binders and water in the early stages of curing, and how it results in changes in dielectric behavior and ion mobility. Our study thus contributes to the widely-studied, ongoing concern in the domain regarding metal carboxylates in historical oil paintings – both in terms of their formation and their role in the stability of the paint and/or its degradation (Casadio, Keune, et al, 2019) – and the role played by water.

Preliminary results related to differently treated oils (namely, cold pressed linseed oil, stand oil and leaded oil) subjected to different relative humidity conditions will be presented. A multi-analytical protocol including FTIR spectroscopy, GC-MS and acid values measurements, has been developed to fully characterize the chemical state of the different oil systems and highlight links between chemical changes and the dielectric properties of these materials, characterized using a Vector Network Analyzer (VNA) methodology. Attention has been given to the very early stages of curing and the obtained results connected to findings from food science (Ghnimi et al, 2017; El-Shami et al, 1992) and engineering (Zhang et al, 2023). Additionally, Dynamic Vapour Sorption (DVS) was used to evaluate variations in the water sorption behaviour of the oils under investigation, and to explore how these relate to their dielectric and chemical properties.

Acknowledgement: this work is realised in the framework  of the EEHOP project funded by the FNRS (Research fund for Scientific Research, Belgium), grant number n° 1.0519.24 « Exploring metal carboxylate-related electrical properties and ionic processes in oil paint films: fundamental insights into historical oil paintings’ degradation processes”.

Bibliography:

Francesca Casadio, Katrien Keune, Petria Noble, Annelies Van Loon, Ella Hendriks, Silvia A. Centeno, Gillian Osmond (2019), Metal Soaps in Art – Conservation and Research. Springer Cham. https://doi.org/10.1007/978-3-319-90617-1

El-Shami, S.M., Selim, I.Z., El-Anwar, I.M. and El-Mallah, M.H. (1992), Dielectric properties for monitoring the quality of heated oils. J Am Oil Chem Soc, 69: 872-875. https://doi.org/10.1007/BF02636335

Ghnimi, S., Budilarto, E. and Kamal-Eldin, A. (2017), The New Paradigm for Lipid Oxidation and Insights to Microencapsulation of Omega-3 Fatty Acids. Comprehensive Reviews in Food Science and Food Safety, 16: 1206-1218. https://doi.org/10.1111/1541-4337.12300

Zhang, T.; Chen, M.; Zhou, H.; Shi, G.; Fan, X.; Wu, Q. Study on the Anti-Aging Performance of Different Nano-Modified Natural Ester Insulating Oils Based on Molecular Dynamics. Nanomaterials 2023, 13, 653. https://doi.org/10.3390/nano13040653