## Slide 1
Qi Chen1, Valeriya Kilchytska1, Léopold Van Brandt1, Eva Bestelink2, Radu A. Sporea2, Denis Flandre1
1 ICTEAM, UCLouvain, Louvain-la-Neuve 1348, Belgium
2ATI, University of Surrey, Guildford, United Kingdom
10th Joint EuroSOI Workshop and International Conference on Ultimate Integration on Silicon 2024
Low-frequency Noise in Polysilicon Source-Gated Transistors
Athens, May 17, 2024

## Slide 2
Low-frequency Noise in Polysilicon Source-Gated Thin-Film Transistor
2
J. M. Shannon et al., IEEE Electron Device Lett., 2003.
Advantages
Low saturation voltage
High intrinsic gain
Reduced short-channel effects
Polysilicon Source-gated Transistors (SGT)
Applications
Amplifiers
Drive circuit for displays
Trade-off
Lower current output for the same gate bias and device dimensions due to the Schottky barrier
Why polysilicon?
Balanced cost and electrical characteristics for thin-film large-area circuit applications
Radu A. Sporea et al., IEEE Trans. Electron Devices, 2010

## Slide 3
Low-frequency Noise (LFN) in transistors
McWhorter model (Carrier Number Fluctuation (CNF) model)
Low-frequency Noise in Polysilicon Source-Gated Thin-Film Transistor
Angeliki Tataridou, PhD Dissertation, 2022.
Hooge model (Carrier Mobility Fluctuation (CMF) model)
Low-frequency noise models
3
G. Ghibaudo et al., Microelectron. Reliab., 2002
with
Hooge parameter
Trap density
Notes: The downsizing of the geometrical dimensions, which enhance the performance and speed of transistors, Low Frequency Noise has become a major concern for nanoscale transistors as its impact on both device and circuit level is more important than ever

## Slide 4
Objective and Outline
DC Characteristics of Polysilicon SGT
LFN Characteristics of Polysilicon SGT
Conclusion and prospects
Low-frequency Noise in Polysilicon Source-Gated Thin-Film Transistor
Understanding the source of low-frequency noise in polysilicon SGT
4

## Slide 5
Low-frequency Noise in Polysilicon Source-Gated Thin-Film Transistor
1.1. Device structure
Schematic of the measured device and measurement configurations
5
Gate
Ohmic
Contact
SiO2
field plate
SiO2
Polysilicon
120 nm
40 nm
300 nm
4 μm
4 μm
Schottky
Contact
Ohmic
Contact
Source
Drain
Source
Drain
SGT configuration
TFT configuration
Bulk doping dose: 0.5 ×1012 cm-2 & 1.5 ×1012 cm-2

## Slide 6
Doping Dose = 0.5 ×1012 cm-2
Transfer curves of SGT and TFT configuration
Low-frequency Noise in Polysilicon Source-Gated Thin-Film Transistor
1.2. IV measurements
On-state current increases by two orders of magnitude in TFT configuration
6
Output curves of SGT
VGS ranges from 20 to -4 V, -4V per step
Saturation region
Linear region
Doping Dose = 0.5 ×1012 cm-2
Bias points @ VD = 5 V
Typical SGT output curves with low saturation voltages and low output conductance
Notes: Extracted mobility μ = 53 cm·V-1s-1 SGT SS = 0.8 V/dec TFT SS = 1.1 V/dec
The bahvaior off-state and subthreshold region is dominated by the channel like in the FET. The negative bias stress normally yields a negative threshold voltage shift of the thin film transistors due to the additional positive charges trapped in the gate dielectrics or at channel/gate insulator interface.

## Slide 7
Low-frequency Noise in Polysilicon Source-Gated Thin-Film Transistor
1.3. TCAD Simulations
Parameter | Value
Schottky barrier height | 0.35 eV
Mobility | 20 cm·V-1s-1
Permittivity | 11.7
Fixed charge density Qf | 4×1011 cm-2
Acceptor defect density Dit | 1×1012 cm-3
Key parameters used in simulations
Schematic simulated device structure
Drain
Drain
SiO2
Schottky Source with field plate
Gate
SiO2
Polysilicon
7
Doping Dose = 0.5 ×1012 cm-2
VGS ranges from 0 to 20 V, 5V per step
Doping Dose = 0.5 ×1012 cm-2
Simulated IV characteristics
Ich
Ich
Ibarrier

## Slide 8
Low-frequency Noise in Polysilicon Source-Gated Thin-Film Transistor
1.3. TCAD Simulations
Transfer and (gm/ID)2 curves at different doping concentrations
8
Decreased doping concentration
SS model for accumulation-mode
device
Decreased doping concentration
VGS –VT = -6 V
VGS –VT = -4 V
VGS –VT = -2 V
VGS –VT = 0 V
VGS –VT = 2 V
Log (Current Density) (A/cm2)
0
3
2
1
4
Variation of current densities
Source Region
Channel
Source Region
Channel
1e17 cm-3
2e17 cm-3

## Slide 9
Low-frequency Noise in Polysilicon Source-Gated Thin-Film Transistor
2.1. LFN measurement
The LFN noise behavior are confirmed with the PSD approximately proportional to 1/f
PSD increases with gate voltage in
subthreshold region
9
Power spectral density (PSD) SId under different doping and fixed current in Schottky configuration
Doping Dose = 0.5 ×1012 cm-2
Doping Dose = 1.5 ×1012 cm-2
f -1
VD = 5 V
VD = 5 V
f -1
f -0.83
f -0.82
f -0.86
f -0.87
f -0.9
f -0.96
f -0.91
f -0.87
f -0.81
f -0.85
f -0.86
f -0.9
f -0.9
f -0.9
with λ = - 0.7 ~ -1.3
SId ~ f λ

## Slide 10
Low-frequency Noise in Polysilicon Source-Gated Thin-Film Transistor
2.2. Analysis of LFN in Ohmic configuration
PSD varies as the reciprocal of ID indicating that the noise in subthreshold region originates from
carrier mobility fluctuation, as in previous reported polysilicon transistor.
ID-1
ID-1
10
Normalized Sid versus ID of Ohmic configuration
Carrier Mobility Fluctuation (CMF) model
G. Ghibaudo et al., Microelectron. Reliab., 2002
A. Mercha, et al., Journal of Applied Physics, 2001
αh ~ 2.5 ×10 -3

## Slide 11
Low-frequency Noise in Polysilicon Source-Gated Thin-Film Transistor
2.3. Analysis of LFN in Schottky configuration
The normalized PSD at high ID are proportional to (gm/ID)2, indicating the domination of CNF model
The normalized PSD at low ID are proportional to ID-1, indicating the domination of CMF model
The plateau can be explained by the variation of buried channel position in subthreshold region
VD = 0.5 V
VD = 5 V
11
Normalized Sid and (gm/ID)2 versus ID of Schottky configuration
ID-1
Carrier Number Fluctuation (CNF) model
with
ID-1
~ 7 × 10-8 V2/Hz
Notes: Nt ~ 2.46 × 1019 eV/cm3

## Slide 12
Low-frequency Noise in Polysilicon Source-Gated Thin-Film Transistor
3. Conclusion and prospects
The variation of buried channel position with gate voltages in high doping case causes a second plateau in the (gm/ID)2
Is CNF due to the barrier current control in SGT in high ID/VG regime? To be probed further by studying the impact of
Source length
Schottky barrier height
12
Configuration | LFN Model
Ohmic | CMF
Schottky | CMF at low ID
 | CNF at high ID

## Slide 13
Thank you !
10th Joint EuroSOI Workshop and International Conference on Ultimate Integration on Silicon 2024
13