## Slide 1
Roughness vs. Sub-Surface Porosity
Key Factors in Fatigue Behavior of AlSi10Mg LPBF Alloy
van der Rest, Camille and Poncelet, Olivier and Manzano Navarrete, Rodrigo Arturo and Simar Aude.
Leuven Additive Manufacturing Conference 2025
27-28 mai

## Slide 2
Poncelet et. al, 2021
Critical assessment of the impact of process parameters on vertical roughness and hardness of thin walls of AlSi10Mg processed by laser powder bed fusion
Additive Manufacturing
TED contour = TED bulk
TED contour >> TED bulk
High roughness
low porosity
Low roughness
High porosity
TED = Power / speed
Roughness or sub-surface porosities?
2/14

## Slide 3
Roughness:
Sub-surface porosity:
Microstructure:
540 µm
540 µm
540 µm
Contour TED
Any trade-off?
high
low
homogeneous
Roughness:
Sub-surface porosity :
Microstructure:
medium
low
inhomogeneous
Roughness:
Sub-surface porosity :
Microstructure:
very low
high
inhomogeneous
4
Materials and methods
Results and discussion
Conclusion
Context and aims
3/14

## Slide 4
Manufacturing of tensile and fatigue samples
Fatigue properties
Crack initiation analysis

## Slide 5
Powder : 70% recycled AlSi10Mg + 30% new
ASTM E8/E8M-15a and ASTM E466-15
4
Materials and methods
Results and discussion
Conclusion
Context and aims
3 sets of parameters involved
60 mm
Parameters – 30 µm layer – 100 µm hatch |  | 
Name | Contours First | Bulk
Rough | 230 W at 1200 mm/s | 230 W at 1200 mm/s
Smooth | 270 W at 600 mm/s | 230 W at 1200 mm/s
Smooth+KHP | 270 W at 300 mm/s | 230 W at 1200 mm/s
X200 from 3D-systems
5/14
Stress release heat treatment (SRHT): 2h at 250°C

## Slide 6
4
Materials and methods
Results and discussion
Conclusion
Context and aims
Targetted « defects »
High Roughness
Medium Roughness
Low
Roughness
Inhomogeneous
microstructure
Inhomogeneous
microstructure
Sub-surface porosity
Poncelet et. al, 2021
Critical assessment of the impact of process parameters on vertical roughness and hardness of thin walls of AlSi10Mg processed by laser powder bed fusion
Additive Manufacturing
6/14
Rough
Smooth
Smooth + KHP

## Slide 7
Post-treatment
Polishing: from SiC 320 to 1/4 μm, removing +-100 µm of the diameter
Sandblasting (SB): made of 98% of Al2O3, with d50 = 445 µm for adding compressive stress
4
Materials and methods
Results and discussion
Conclusion
Context and aims
Rough
Smooth
Smooth+KHP
7/14
As-built

## Slide 8
Post-treatment
4
Materials and methods
Results and discussion
Conclusion
Context and aims
8/14
As-built
Polished
Sand blasted
3 surface states - On a Smooth sample here

## Slide 9
We obtained the expected defects
Materials and methods
Results and discussion
Conclusion
Context and aims
µCT
9/14
Roughness (EN ISO 4288 )
Rough
Smooth
Smooth + KHP

## Slide 10
Materials and methods
Results and discussion
Conclusion
Context and aims
Static properties
 | Yield Strength, 0.2% [MPa] | Ultimate Tensile Strength [MPa] | Elongation at break [/]
Rough | 239 | 404 | 0.04
Smooth | 244 | 413 | 0.04
Smooth with KHP | 239 | 392 | 0.03
L0 = 20 mm – Crosshead speed= 1mm/min
10/14

## Slide 11
Fatigue properties
30 Hz – R = 0.1
Initiation: Surface (roughness), Lack-of-fusion, Keyhole, porosity, undefined bulk defects
Materials and methods
Results and discussion
Conclusion
Context and aims
11/14

## Slide 12
Initiation crack sites
Materials and methods
Results and discussion
Conclusion
Context and aims
Rough: multiple sites
Smooth: single site
Smooth+KHP: single site
12/14
Rough
Smooth+KHP
Low = 140 and 160 Mpa Medium= 180 MPa High = 200 and 220 MPa

## Slide 13
Initiation crack sites
Low = 140 and 160 Mpa Medium= 180 MPa High = 200 and 220 MPa
Materials and methods
Results and discussion
Conclusion
Context and aims
13/14

## Slide 14
4
Materials and methods
Results and discussion
Conclusion
Context and aims
Conclusion
Roughness is more detrimental in fatigue than sub-surface porosity
Higher roughness leads to multiple initiation sites and thus early break
Keyholes in contours are still better than roughness
Polishing brings sub-surface porosity to the surface
Sand blasting is the best post-treatment here
Non-optimized (rough) samples are the worst in any cases