## Slide 1
Alexis André
1. SMaRT, Department of Chemical Engineering, KU Leuven, Leuven, Belgium
2. BSMA/IMCN, Université catholique de Louvain, Louvain-la-Neuve, Belgium
Promotors : Christian Clasen1, Evelyne Van Ruymbeke2
“Investigating the linear and nonlinear rheology of model
polymer melts”

## Slide 2
What is a polymer ?
2
Dynamic and reconfigurable materials from reversible network interactions
https://www.bbau.ac.in/dept/Chemistry/TM/MCH%20301%20Superamolecular%20Chemistry%20DoC.pdf
https://olsenlab.mit.edu/research/dynamics/#:~:text=Associative%20polymers%20contain%20sticky%20groups,responsive%20and%20self%2Dhealing%20abilities.
Rubinstein, M., and A. N. Semenov, “Dynamics of entangled solutions of associating polymers,” Macromolecules 34, 1058–1068 (2001)
Poly + mer, from Ancient Greeks πολύς (polus) ‘many’ and μέρος (meros) ‘part’
Polymers are macromolecules made of many « monomers »
Polystyrene
Synthetic polymer
Natural polymer
DNA
Natural latex
times
Monomer
“Investigating the linear and nonlinear rheology of model polymer melts”
Let's break down the title into different parts…
Silk spider
Nylon

## Slide 3: Diverse processing methods
Inkjet printing process
In polymer industry, melt processing is widely used
Main steps are :
      Heating
      Flowing
      Shaping
      Cooling
Film Blowing
Melt spinning
3D printing
Int
Stretch blow molding
[1] T. Shahid, PhD thesis, UCLouvain (2018).
[2] Downloaded on 21/06/2019 from https://www.britannica.com/technology/melt-spinning-materials-processing
[3] Downloaded on 25/09/2019 from https://robinsonpackaging.com/plastic-packaging/injection-stretch-blow-moulding/
[4] C. Bailly, E. Van Ruymbeke, Transparent du cours « LMAPR2018 : Rheometry and Polymer Processing »., 2018-2019,
3
Deformation
Polymers are light, easy to process and to incorporate into a variety of forms
Notes: Models based on the models given in class for the shear and elongational flow.
For the shear flow : the lower plate stays still while the upper one moves. So v_x(0) = 0. The flow is established so the only velocity (in 2D) is parallel to the plates and varies only along x (stationary flow, each cross section, same velocity profile).
For shear flow : 1D example shown. Velocity of center doesn’t change. The rest is strtched proportionally to the strain rate (called hecnky strain rate). Of course, since 1D, only 1 velocity component depending on one direction.
Both can be generalized in 3D.

## Slide 4: Diverse processing methods
Inkjet printing process
In polymer industry, melt processing is widely used
Main steps are :
      Heating
      Flowing
      Shaping
      Cooling
Film Blowing
Melt spinning
3D printing
Int
Stretch blow molding
[1] T. Shahid, PhD thesis, UCLouvain (2018).
[2] Downloaded on 21/06/2019 from https://www.britannica.com/technology/melt-spinning-materials-processing
[3] Downloaded on 25/09/2019 from https://robinsonpackaging.com/plastic-packaging/injection-stretch-blow-moulding/
[4] C. Bailly, E. Van Ruymbeke, Transparent du cours « LMAPR2018 : Rheometry and Polymer Processing »., 2018-2019,
4
Polymers are light, easy to process and to incorporate into a variety of forms
Deformation
Stress
Deformation
Control of the flow:
Notes: Models based on the models given in class for the shear and elongational flow.
For the shear flow : the lower plate stays still while the upper one moves. So v_x(0) = 0. The flow is established so the only velocity (in 2D) is parallel to the plates and varies only along x (stationary flow, each cross section, same velocity profile).
For shear flow : 1D example shown. Velocity of center doesn’t change. The rest is strtched proportionally to the strain rate (called hecnky strain rate). Of course, since 1D, only 1 velocity component depending on one direction.
Both can be generalized in 3D.

## Slide 5
Shear and extensional flow
5
Dynamic and reconfigurable materials from reversible network interactions
https://www.bbau.ac.in/dept/Chemistry/TM/MCH%20301%20Superamolecular%20Chemistry%20DoC.pdf
Rubinstein, M., and A. N. Semenov, “Dynamics of entangled solutions of associating polymers,” Macromolecules 34, 1058–1068 (2001)
Polymer processing techniques are generally dominated either by shear or extension
Extensional flow
Shear flow
Measurements with a rotational rheometer
Measurements with a Filament stretching rheometer

## Slide 6: Linear and nonlinear rheology
Tapez une équation ici.
Tapez une équation ici.
Int
6
What is happening at the molecular level?
Costanzo et al. Macromol. 2016
PS melts
PS melts
Nielsen et al. J. Rheol. 2006
“Investigating the linear and nonlinear rheology of model polymer melts”
Linear rheology
Non linear regime
Flow deforms chains faster that they can relax
Change of due to change of microstructure
Theories generally fail in this regime
&
Tapez une équation ici.
= cst
Theories generally fail in this regime
Theories generally fail in this regime
Microstructure is at equilibrium
Shear thickening fluid (Pourquoi ?)
My focus : What is happening
at the molecular level?
Notes: Models based on the models given in class for the shear and elongational flow.
For the shear flow : the lower plate stays still while the upper one moves. So v_x(0) = 0. The flow is established so the only velocity (in 2D) is parallel to the plates and varies only along x (stationary flow, each cross section, same velocity profile).
For shear flow : 1D example shown. Velocity of center doesn’t change. The rest is strtched proportionally to the strain rate (called hecnky strain rate). Of course, since 1D, only 1 velocity component depending on one direction.
Both can be generalized in 3D.

## Slide 7: Outline
Int
7
My PhD consist of two main parts:
Entangled polymer melts
Supramolecular polymers
Orthogonal superposition rheology
1. Characterisation and modeling
2. Design of a rheometer
Notes: Models based on the models given in class for the shear and elongational flow.
For the shear flow : the lower plate stays still while the upper one moves. So v_x(0) = 0. The flow is established so the only velocity (in 2D) is parallel to the plates and varies only along x (stationary flow, each cross section, same velocity profile).
For shear flow : 1D example shown. Velocity of center doesn’t change. The rest is strtched proportionally to the strain rate (called hecnky strain rate). Of course, since 1D, only 1 velocity component depending on one direction.
Both can be generalized in 3D.

## Slide 8: Outline
Int
8
Entangled polymer melts
Supramolecular polymers
Orthogonal superposition rheology
1. Characterisation and modeling
2. Design of a rheometer
My PhD consist of two main parts:
Notes: Models based on the models given in class for the shear and elongational flow.
For the shear flow : the lower plate stays still while the upper one moves. So v_x(0) = 0. The flow is established so the only velocity (in 2D) is parallel to the plates and varies only along x (stationary flow, each cross section, same velocity profile).
For shear flow : 1D example shown. Velocity of center doesn’t change. The rest is strtched proportionally to the strain rate (called hecnky strain rate). Of course, since 1D, only 1 velocity component depending on one direction.
Both can be generalized in 3D.

## Slide 9
Rheology of entangled polymers
9
Dynamic and reconfigurable materials from reversible network interactions
https://www.bbau.ac.in/dept/Chemistry/TM/MCH%20301%20Superamolecular%20Chemistry%20DoC.pdf
https://olsenlab.mit.edu/research/dynamics/#:~:text=Associative%20polymers%20contain%20sticky%20groups,responsive%20and%20self%2Dhealing%20abilities.
Rubinstein, M., and A. N. Semenov, “Dynamics of entangled solutions of associating polymers,” Macromolecules 34, 1058–1068 (2001)
  Polymer are long and flexible chains
1
3.4
Macaroni
Spaghetti
How do scientists visualize polymers ?
  Polymer chains entangle

## Slide 10: The tube model in the linear regime
Entanglements confine each chain in a tube-like region with a lifetime
3 parameters suffice to describe entirely the spectrum of relaxation times
Network stress-scale
Network timescale
Linear response of entangled polymers
Test chain entangled
Tube model
Huang et al. Macromol. 2013
Doi & Edwards, 1986.
Number of entanglements
Tube-like motion of a DNA molecule
Perkins, T.; Smith, D.; Chu, S. Science, 1994
Notes: For shear flow : 1D example shown. Velocity of center doesn’t change. The rest is strtched proportionally to the strain rate (called hecnky strain rate). Of course, since 1D, only 1 velocity component depending on one direction.
Both can be generalized in 3D.

## Slide 11
Flow competes with spectrum of relaxation time
Experimental results
I
II
III
IV
Prediction as per DEMG model
This view fails in the non-linear regime…
The tube model in the nonlinear regime
Huang et al. Macromol. 2013
Notes: Models based on the models given in class for the shear and elongational flow.
For the shear flow : the lower plate stays still while the upper one moves. So v_x(0) = 0. The flow is established so the only velocity (in 2D) is parallel to the plates and varies only along x (stationary flow, each cross section, same velocity profile).
For shear flow : 1D example shown. Velocity of center doesn’t change. The rest is strtched proportionally to the strain rate (called hecnky strain rate). Of course, since 1D, only 1 velocity component depending on one direction.
Both can be generalized in 3D.

## Slide 12: Extension of the tube model to NLVE
Potential causes :
When , local environment becomes anisotropic
reduction of the monomeric friction
reduction of and
1. Alignement - Induced reduction of the monomeric friction
2. Deviation from the fluctuation dissipation theorem
12
Introduction
with
Molecular dynamics simulations
Ianniruberto & Marrucci, Macromol. 2020
Yaoita et al., Macromol. 2012
Matsumiya & Watanabe, Prog. Polym. Sci. 2020
Notes: Models based on the models given in class for the shear and elongational flow.
For the shear flow : the lower plate stays still while the upper one moves. So v_x(0) = 0. The flow is established so the only velocity (in 2D) is parallel to the plates and varies only along x (stationary flow, each cross section, same velocity profile).
For shear flow : 1D example shown. Velocity of center doesn’t change. The rest is strtched proportionally to the strain rate (called hecnky strain rate). Of course, since 1D, only 1 velocity component depending on one direction.
Both can be generalized in 3D.

## Slide 13: Extension of the tube model to NLVE
13
Extensional rheology of entangled polymer melts
Tapez une équation ici.
Extensional viscosity of polymeric solutions
Filament Stretching Rheometer (FSR)
www.rheofilament.com (September 18, 2021)
Notes: Models based on the models given in class for the shear and elongational flow.
For the shear flow : the lower plate stays still while the upper one moves. So v_x(0) = 0. The flow is established so the only velocity (in 2D) is parallel to the plates and varies only along x (stationary flow, each cross section, same velocity profile).
For shear flow : 1D example shown. Velocity of center doesn’t change. The rest is strtched proportionally to the strain rate (called hecnky strain rate). Of course, since 1D, only 1 velocity component depending on one direction.
Both can be generalized in 3D.

## Slide 14: Outline
Change of scaling laws in agreement with reduction :
with
Dilution makes the environment less anisotropic
Polymeric solutions
Bimodal systems
Changing does not affect significantly the anisotropy of the environment
with
Extensional rheology of entangled polymer melts
Extensional viscosity of bimodal melts
Chain stretching
when

## Slide 15: Outline
Int
15
My PhD consist of three parts:
Entangled polymer melts
Supramolecular polymers
Orthogonal superposition rheology
1. Characterisation and modeling
2. Design of a rheometer
Notes: Models based on the models given in class for the shear and elongational flow.
For the shear flow : the lower plate stays still while the upper one moves. So v_x(0) = 0. The flow is established so the only velocity (in 2D) is parallel to the plates and varies only along x (stationary flow, each cross section, same velocity profile).
For shear flow : 1D example shown. Velocity of center doesn’t change. The rest is strtched proportionally to the strain rate (called hecnky strain rate). Of course, since 1D, only 1 velocity component depending on one direction.
Both can be generalized in 3D.

## Slide 16
Supramolecular chemistry : Transient polymer networks
16
« Chemistry beyond the molecule » : The supramolecular interactions
Dynamic and reconfigurable materials from reversible network interactions
https://www.bbau.ac.in/dept/Chemistry/TM/MCH%20301%20Superamolecular%20Chemistry%20DoC.pdf
https://olsenlab.mit.edu/research/dynamics/#:~:text=Associative%20polymers%20contain%20sticky%20groups,responsive%20and%20self%2Dhealing%20abilities.
Physical bonds vs chemical bonds
Rubinstein, M., and A. N. Semenov, “Dynamics of entangled solutions of associating polymers,” Macromolecules 34, 1058–1068 (2001)
Adapted from Wiley Interdiscip. Rev. Nanomed. Nanobiotechnol. 2013, 5, 582-621.
Introduction of inter-chain interactions into polymers
Reproduced from Wu, S.; Chen, Q. Macromolecules 2022, 55, 697–714.

## Slide 17
Supramolecular chemistry : Transient polymer networks
17
Dynamic and reconfigurable materials from reversible network interactions
https://www.bbau.ac.in/dept/Chemistry/TM/MCH%20301%20Superamolecular%20Chemistry%20DoC.pdf
https://olsenlab.mit.edu/research/dynamics/#:~:text=Associative%20polymers%20contain%20sticky%20groups,responsive%20and%20self%2Dhealing%20abilities.
Rubinstein, M., and A. N. Semenov, “Dynamics of entangled solutions of associating polymers,” Macromolecules 34, 1058–1068 (2001)
Many possible applications:
2. Self-healable materials/Super-adhesive
1. Enhancing toughness of materials
:
3. Thermal responsiveness
:
Leibler et al. Nature 2008, 451, 977–980.
Meijer et al. Science 1997, 278, 1601-1604.
Ionic bonds
Covalent bonds
&
:
Suo et al. Nature 2012, 489, 133–136.

## Slide 18
Supramolecular polymers: transient polymer networks
1. Terpyridine (tpy) groups
2. 2-ureido-4[1H]-pyrimidinone (Upy) groups
18
Cui, K. & Gong, J. P. J. Rheol. 2022.
Supramolecular bonds
<
Terpyridine-modified poly(n-butyl acrylate)
+
Metal ions

## Slide 19
Linear Viscoelasticity : - based systems
19
Linear rheology :
Emergence of a rubbery plateau
Changer Magenta -> Rouse
Formation of a dense network
Plate-plate geometries
Delay of the longest relaxation time
Pente
PnBA25k - 11Tpy
Ions

## Slide 20
Linear Viscoelasticity : - based systems
Effect of the nature of ions
Dissociation
vs
Deficiency

## Slide 21
Linear Viscoelasticity : - based systems
Effect of the nature of ions
Dissociation
vs
Segmental motion
Deficiency

## Slide 22
Linear Viscoelasticity : - based systems
Effect of the nature of ions
Dissociation
vs
Dissociation of bonds
Segmental motion
Deficiency
leads to bonds much more stable than does

## Slide 23
Linear Viscoelasticity : Thermal responsiveness
Dissociation
vs
Deficiency
Changing the nature of ions also allows to tune the thermal responsiveness
 | Neutral | Cu(II) | Zn(II)
] | 51.2 | 49.4 | -
 | Neutral | Cu(II) | Zn(II)
 | 51.2 | 49.4 | -

## Slide 24
Linear Viscoelasticity : - based systems
24
Modelling
M :
Dissociation
vs
Unentangled chains : Sticky Rouse model
Entangled chains : Sticky reptation model
Jiang et al. Macromol. 2021
Tube with a lifetime
Baxandall . Macromol. 1988
Doi & Edwards . Theory of polymer dynamics. 1986

## Slide 25
Steady shear measurements : Method
25
Plate-plate geometries
Cone-partitioned-plate geometries
Cone-Partitioned-Plate geometry (CPP)
Cone geometry
Polymer sample
Outer hollowed parallel plate
Inner parallel plate
Translation stages for alignement
Nonlinear shear rheology techniques for polymer melt
Upper flat plate
(Image from : Costanzo et al., Macromolecules, (2016).)

## Slide 26
Steady shear measurements : Method
26
Cone geometry
Polymer sample
Outer hollowed parallel plate
Inner parallel plate
Translation stages for alignement
Nonlinear shear rheology techniques
Inward propagation of edge fracture
CPP measures only the inner part
Plate-plate geometries
Cone-partitioned-plate geometries
Upper flat plate
Cone-Partitioned-Plate geometry (CPP)
(Image from : Costanzo et al., Macromolecules, (2016).)

## Slide 27
Nonlinear Viscoelasticity : - based systems
27
+
Metal Ions
(
Transient strain hardening is revealed
Stretching of the network strands :
PnBA25k – 7tpy
PnBA25k - 7Tpy – 0.75 eq.

## Slide 28
Nonlinear shear rheology: - based systems
28
2. Yield strain independent of
1. Validity of TTS principle
3. Breakdown of the Cox-Merz rule
Experimentally observed features in nonlinear shear regime:

## Slide 29: Outline
Int
29
My PhD consist of three parts:
Entangled polymer melts
Supramolecular polymers
Orthogonal superposition rheology
1. Characterisation and modeling
2. Design of a rheometer
Notes: Models based on the models given in class for the shear and elongational flow.
For the shear flow : the lower plate stays still while the upper one moves. So v_x(0) = 0. The flow is established so the only velocity (in 2D) is parallel to the plates and varies only along x (stationary flow, each cross section, same velocity profile).
For shear flow : 1D example shown. Velocity of center doesn’t change. The rest is strtched proportionally to the strain rate (called hecnky strain rate). Of course, since 1D, only 1 velocity component depending on one direction.
Both can be generalized in 3D.

## Slide 30
Orthogonal superposition (OSP) rheology
30
Objective : Measure the response of polymer melts under orthogonal superposition flow
1
2
3
Spectral analysis of the flow
Hendrickx, J. PhD thesis 2019
Entangled associative polymers
Simu + Linear perturabtion

## Slide 31
Superposition rheology
31
Horizontal shift :
Predictions of orthogonal moduli of an unentangled melts using a bead-spring model from the literature
&
Constitutive model from Sato et al. Phys. Fluid 2021
Predictions of and
Master curves

## Slide 32
OSP design
2. Drive: TA ARES-G2
1. Flow cell: Annular Couette cell
Force rebalance
transducer
Servo-motor
The design is composed of three main components:
3. Shafts
www.tainstruments.com (August 1, 2023)

## Slide 33
Orthogonal superposition (OSP) rheology
33
Simu + Linear perturabtion
Flow cell : Annular Couette flow with inner cylinder rotating and outer cylinder oscillating in axial direction.
Relative error for power-law fluid

## Slide 34: Outline
Conclusion
We were able to model the linear rheology of unentangled and entangled associative polymers using a statistical sticky Rouse model and a home-made sticky reptation model
We obtained scaling laws for entangled melts in nonlinear extensional flow which confirms the hypothesis of reduction:
34
Perspectives
Validate the orthogonal superposition flow cell
Analyse SAXS data of Pr. Kell Mortensen
Writing of the manuscript
We showed characteristic features in the rheology unentangled associative polymers such as constant yield strain, TTS validity and transient hardening.
Tapez une équation ici.
Polymeric solutions
Bimodal melts
We modeled the linear rheology of unentangled and entangled associative polymers using a bead-spring model
and a home-made sticky reptation model.
We observed transient thickening, an yield strain independent of and a confirmation of the validity of TTS for unentangled associative polymers in nonlinear shear.
We proposed and validated by CFD a new design of a rheometer tool to perform OSP measurements

## Slide 35
Acknowledgements
35
Dynamic and reconfigurable materials from reversible network interactions
https://www.bbau.ac.in/dept/Chemistry/TM/MCH%20301%20Superamolecular%20Chemistry%20DoC.pdf
https://olsenlab.mit.edu/research/dynamics/#:~:text=Associative%20polymers%20contain%20sticky%20groups,responsive%20and%20self%2Dhealing%20abilities.
Rubinstein, M., and A. N. Semenov, “Dynamics of entangled solutions of associating polymers,” Macromolecules 34, 1058–1068 (2001)
  Thank you blablabla

## Slide 36
Supramolecular chemistry : Transient polymer networks
36
Dynamic and reconfigurable materials from reversible network interactions
https://www.bbau.ac.in/dept/Chemistry/TM/MCH%20301%20Superamolecular%20Chemistry%20DoC.pdf
https://olsenlab.mit.edu/research/dynamics/#:~:text=Associative%20polymers%20contain%20sticky%20groups,responsive%20and%20self%2Dhealing%20abilities.
Cui, K., and J. P. Gong, J. Rheol. 66, 1093 (2022)
+
: Ligand
Metal ions
« Chemistry beyond the molecule » : The supramolecular interactions
In nature…
Harrington, M. J. et al., Science, 328(5975), 216–220 (2010)
Physical bonds vs chemical bonds

## Slide 37
Supramolecular polymers: transient polymer networks
1. Terpyridine (tpy) groups
37
Supramolecular bonds
Terpyridine-modified poly(n-butyl acrylate)
:
Lability
Chapter 5 and 6
Cui, K. & Gong, J. P. J. Rheol. 2022.

## Slide 38
Linear viscoelasticity: - based networks
38
1. Unentangled polymers
2. Entangled polymers
Large reinforcement
(Chapter 5)
(Chapter 6)
Saturation of and
 | 1 eq. | 0.75 eq. | 0.5 eq. | 0.25 eq. | 0.125 eq.
 | 81.4 | 67.6 | 61.5 | 36.9 | 36.4
 | 1 eq. | 0.75 eq. | 0.5 eq. | 0.25 eq. | 0.125 eq.
 | 81.4 | 67.6 | 61.5 | 36.9 | 36.4
PnBA25k - 11Tpy
PnBA140k - 13Tpy

## Slide 39
Linear viscoelasticity: - based systems
39
0.5 eq.
0.5 eq.
Zn(II) ions are much more labile than Cu(II) ions
PnBA140k - 13Tpy
PnBA25k - 11Tpy
1. Unentangled polymers
2. Entangled polymers
0.5 eq.
0.5 eq.

## Slide 40: Outline
Modeling: the sticky reptation model
40
Leibler, L. et al. Macromol. 1991
Sticky reptation model
Time marching algorithm
1. Reptation
2. Constraint Release
3. Contour Length Fluctuation
van Ruymbeke, E. et al. Macromolecules 2006
3 ingredients for the modelling of entangled supramolecular polymers

## Slide 41: Modeling: the sticky reptation model
0.5 eq.
0.75 eq.
41
PSMA108k – 3.7%Na
PI – 84k – U1
Data from Gold et al. J. Rheol. 2017
Data from Kim et al. Macromolecules 1994
Sticky CLF
Stepwise CLF
The resulting model provides a decent fit of experimental data
Literature data
Notes: Models based on the models given in class for the shear and elongational flow.
For the shear flow : the lower plate stays still while the upper one moves. So v_x(0) = 0. The flow is established so the only velocity (in 2D) is parallel to the plates and varies only along x (stationary flow, each cross section, same velocity profile).
For shear flow : 1D example shown. Velocity of center doesn’t change. The rest is strtched proportionally to the strain rate (called hecnky strain rate). Of course, since 1D, only 1 velocity component depending on one direction.
Both can be generalized in 3D.

## Slide 42
Supramolecular polymers: transient polymer networks
1. Terpyridine (tpy) groups
2. 2-ureido-4[1H]-pyrimidinone (Upy) groups
42
Chapter 5 and 6
Chapter 4
Synthesised by Flanco Zhuge & Rowanne Lyons (UCLouvain)
Synthesised by Jente Verjans (UGent)
Supramolecular bonds
Cui, K. & Gong, J. P. J. Rheol. 2022.

## Slide 43
Linear Viscoelasticity: Upy - based systems
43
Unentangled associative polymers
[]
PBA | PB | PMA
PBA | PB | PMA
()
No significant effect of the backbone on the strength of the physical bonds

## Slide 44
Modeling: the sticky Rouse model
44
Slow dynamics
Fast dynamics
Liu, H. et al . J. Rheol 2022
Modeling of the linear responses using a bead-spring model
+ correction for non-affine fluctuations
PMA – U10

## Slide 45
Modeling: the sticky Rouse model
45
Slow dynamics
Fast dynamics
Liu, H. et al . J. Rheol 2022
Modeling of the linear responses using a bead-spring model
+ correction for non-affine fluctuations
PMA – U10

## Slide 46
Supramolecular chemistry : Transient polymer networks
46
« Chemistry beyond the molecule » : The supramolecular interactions
Stimuli responsive
Self-healing properties
High tunability (Stiffness, toughness & relaxation time)
Formation of a dynamic and reversible polymeric network
Dynamic and reconfigurable materials from reversible network interactions
https://www.bbau.ac.in/dept/Chemistry/TM/MCH%20301%20Superamolecular%20Chemistry%20DoC.pdf
https://olsenlab.mit.edu/research/dynamics/#:~:text=Associative%20polymers%20contain%20sticky%20groups,responsive%20and%20self%2Dhealing%20abilities.
Properties :
Rubinstein, M., and A. N. Semenov, “Dynamics of entangled solutions of associating polymers,” Macromolecules 34, 1058–1068 (2001)
…
(see for example : Seiffert . Adv. Polym. Sci. 2015, 268, 288.)
Cui, K., and J. P. Gong, J. Rheol. 66, 1093 (2022)
Physical bonds vs chemical bonds

## Slide 47
Rheology of entangled polymers
47
Dynamic and reconfigurable materials from reversible network interactions
https://www.bbau.ac.in/dept/Chemistry/TM/MCH%20301%20Superamolecular%20Chemistry%20DoC.pdf
https://olsenlab.mit.edu/research/dynamics/#:~:text=Associative%20polymers%20contain%20sticky%20groups,responsive%20and%20self%2Dhealing%20abilities.
Rubinstein, M., and A. N. Semenov, “Dynamics of entangled solutions of associating polymers,” Macromolecules 34, 1058–1068 (2001)
  1. Rouse model
1
3.4
Macaroni
Spaghetti
2. The tube model
How do scientists visualize polymers ?

## Slide 48
Supramolecular chemistry : Transient polymer networks
48
Dynamic and reconfigurable materials from reversible network interactions
https://www.bbau.ac.in/dept/Chemistry/TM/MCH%20301%20Superamolecular%20Chemistry%20DoC.pdf
https://olsenlab.mit.edu/research/dynamics/#:~:text=Associative%20polymers%20contain%20sticky%20groups,responsive%20and%20self%2Dhealing%20abilities.
Rubinstein, M., and A. N. Semenov, “Dynamics of entangled solutions of associating polymers,” Macromolecules 34, 1058–1068 (2001)
  Associative polymers

## Slide 49
Supramolecular chemistry : Transient polymer networks
49
Dynamic and reconfigurable materials from reversible network interactions
https://www.bbau.ac.in/dept/Chemistry/TM/MCH%20301%20Superamolecular%20Chemistry%20DoC.pdf
https://olsenlab.mit.edu/research/dynamics/#:~:text=Associative%20polymers%20contain%20sticky%20groups,responsive%20and%20self%2Dhealing%20abilities.
Rubinstein, M., and A. N. Semenov, “Dynamics of entangled solutions of associating polymers,” Macromolecules 34, 1058–1068 (2001)
  Conclusion

## Slide 50: Rouse and tube models
The Rouse model
Stress depends on the orientation of the polymeric chains
After a step strain, chains need to renew their conformation to relax
Relaxation in a time
Unentangled polymer
50

## Slide 51
Supramolecular chemistry : Transient polymer networks
51
Dynamic and reconfigurable materials from reversible network interactions
https://www.bbau.ac.in/dept/Chemistry/TM/MCH%20301%20Superamolecular%20Chemistry%20DoC.pdf
https://olsenlab.mit.edu/research/dynamics/#:~:text=Associative%20polymers%20contain%20sticky%20groups,responsive%20and%20self%2Dhealing%20abilities.
Rubinstein, M., and A. N. Semenov, “Dynamics of entangled solutions of associating polymers,” Macromolecules 34, 1058–1068 (2001)
Many possible applications
2. Self-healable materials/Super-adhesive
1. Enhancing toughness of materials
:
o
H
N
3. Thermal responsiveness
:
Leibler et al. Nature 2008, 451, 977–980.
Meijer et al. Science 1997, 278, 1601-1604.
Ionic bonds
Covalent bonds
&
:
Suo et al. Nature 2012, 489, 133–136.

## Slide 52
Modelling : the Rouse model
52
Distribution of stickers and molar mass
Rouse model in linear flow
Connectivity matrix
Friction force
with
Brownian force
Dissipation-Fluctuation correlation
Jiang et al. Macromol. 2021

## Slide 53: The Rouse model
Int
[5]
with
The Rouse model :
Scaling laws
53
Unentangled PnBA (27 kg/mol)
Notes: Models based on the models given in class for the shear and elongational flow.
For the shear flow : the lower plate stays still while the upper one moves. So v_x(0) = 0. The flow is established so the only velocity (in 2D) is parallel to the plates and varies only along x (stationary flow, each cross section, same velocity profile).
For shear flow : 1D example shown. Velocity of center doesn’t change. The rest is strtched proportionally to the strain rate (called hecnky strain rate). Of course, since 1D, only 1 velocity component depending on one direction.
Both can be generalized in 3D.

## Slide 54
Supramolecular chemistry : Transient polymer networks
54
« Chemistry beyond the molecule » : The supramolecular interactions
Dynamic and reconfigurable materials from reversible network interactions
https://www.bbau.ac.in/dept/Chemistry/TM/MCH%20301%20Superamolecular%20Chemistry%20DoC.pdf
https://olsenlab.mit.edu/research/dynamics/#:~:text=Associative%20polymers%20contain%20sticky%20groups,responsive%20and%20self%2Dhealing%20abilities.
Physical bonds vs chemical bonds
Rubinstein, M., and A. N. Semenov, “Dynamics of entangled solutions of associating polymers,” Macromolecules 34, 1058–1068 (2001)
Adapted from Wiley Interdiscip. Rev. Nanomed. Nanobiotechnol. 2013, 5, 582-621.
Introduction of inter-chain interactions into polymers
Reproduced from Wu, S.; Chen, Q. Macromolecules 2022, 55, 697–714.

## Slide 55
Supramolecular chemistry : Transient polymer networks
55
Dynamic and reconfigurable materials from reversible network interactions
https://www.bbau.ac.in/dept/Chemistry/TM/MCH%20301%20Superamolecular%20Chemistry%20DoC.pdf
https://olsenlab.mit.edu/research/dynamics/#:~:text=Associative%20polymers%20contain%20sticky%20groups,responsive%20and%20self%2Dhealing%20abilities.
Rubinstein, M., and A. N. Semenov, “Dynamics of entangled solutions of associating polymers,” Macromolecules 34, 1058–1068 (2001)
Many possible applications
2. Self-healable materials/Super-adhesive
1. Enhancing toughness of materials
:
o
H
N
3. Thermal responsiveness
:
Suo et al. Nature 2012, 489, 133–136.
Leibler et al. Nature 2008, 451, 977–980.
Meijer et al. Science 1997, 278, 1601-1604.
Ionic bonds
Covalent bonds
&

## Slide 56
Material of interest
56
Dynamic and reconfigurable materials from reversible network interactions
https://www.bbau.ac.in/dept/Chemistry/TM/MCH%20301%20Superamolecular%20Chemistry%20DoC.pdf
https://olsenlab.mit.edu/research/dynamics/#:~:text=Associative%20polymers%20contain%20sticky%20groups,responsive%20and%20self%2Dhealing%20abilities.
Physical bonds vs chemical bonds
How can we assess the network dynamics of supramolecular polymers?
<
M :
Terpyridine-modified poly(n-butyl acrylate)
Adapted from Wiley Interdiscip. Rev. Nanomed. Nanobiotechnol. 2013, 5, 582-621.
+
Metal ions
Group of Pr. Charles-André Fustin

## Slide 57
Linear Viscoelasticity : - based systems
57
Method :
Emergence of a rubbery plateau
Changer Magenta -> Rouse
Formation of a dense network
Plate-plate geometries
Delay of the longest relaxation time
Pente
PnBA25k - 11Tpy
Ions

## Slide 58
Linear Viscoelasticity : - based systems
Effect of the nature of ions
Dissociation
vs
Deficiency

## Slide 59
Linear Viscoelasticity : - based systems
Effect of the nature of ions
Dissociation
vs
Segmental motion
Deficiency

## Slide 60
Linear Viscoelasticity : - based systems
Effect of the nature of ions
Dissociation
vs
Dissociation of bonds
Segmental motion
Deficiency
leads to bonds much more stable than does

## Slide 61
Linear Viscoelasticity : - based systems
61
Modelling
M :
Dissociation
vs
Unentangled chains : Sticky Rouse model
Entangled chains : Sticky reptation model
Jiang et al. Macromol. 2021
Tube with a lifetime
Baxandall . Macromol. 1988
Doi & Edwards . Theory of polymer dynamics. 1986

## Slide 62
Nonlinear Viscoelasticity : - based systems
62
Yield strain
Transient strain hardening is revealed
Stretching of the network strands :

## Slide 63
Nonlinear Viscoelasticity : - based systems
63
Yield strain
Thermal dissociation
Force-induced dissociation
Strain controlled
Strain-rate controlled

## Slide 64
Orthogonal superposition (OSP) rheology
64
Measure the response of polymer melts under orthogonal superposition flow
1
2
3
Spectral analysis of the flow
Information on chain conformations
Investigation in the nonlinear regime
[1] Jan Hendrickx, PhD thesis
Entangled associative polymers
[1]
Simu + Linear perturabtion

## Slide 65: The tube model
Int
Entangled polymer
Modelling of the surrounding chains by a tube
Relaxation in a time
65
Notes: Models based on the models given in class for the shear and elongational flow.
For the shear flow : the lower plate stays still while the upper one moves. So v_x(0) = 0. The flow is established so the only velocity (in 2D) is parallel to the plates and varies only along x (stationary flow, each cross section, same velocity profile).
For shear flow : 1D example shown. Velocity of center doesn’t change. The rest is strtched proportionally to the strain rate (called hecnky strain rate). Of course, since 1D, only 1 velocity component depending on one direction.
Both can be generalized in 3D.

## Slide 66: The tube model
Int
3 mechanisms : Orientation relaxation (LVE)
1. Reptation
2. Contour Length Fluctuation (CLF)
3. Thermal Constraint Release
Relaxation in a time
Zero-shear viscosity
Scaling laws
66
Entangled PS (820 kg/mol - 30wt%)
Notes: Models based on the models given in class for the shear and elongational flow.
For the shear flow : the lower plate stays still while the upper one moves. So v_x(0) = 0. The flow is established so the only velocity (in 2D) is parallel to the plates and varies only along x (stationary flow, each cross section, same velocity profile).
For shear flow : 1D example shown. Velocity of center doesn’t change. The rest is strtched proportionally to the strain rate (called hecnky strain rate). Of course, since 1D, only 1 velocity component depending on one direction.
Both can be generalized in 3D.

## Slide 67
Orthogonal superposition (OSP) rheology
67
Simu + Linear perturabtion
Upper shaft
Lower shaft
Flow cell
Small axial
Amplitude oscillation
Large steady state
rotation
Flow cell : Annular Couette flow with inner cylinder rotating and outer cylinder oscillating in axial direction.

## Slide 68
Design of an Orthogonal Superposition Rheometer
68
Loading of the cell
Bubbles
Concentricity
Problems

## Slide 69
Conclusion
69
Sticky Reptation model with a “delayed CLF” fits the data well in the Rouse and the terminal regime but is less successful in the rubbery plateau
Associative systems can be used to tune and
Sticky Rouse model fits well unentangled associative in the Rouse
Nonlinear viscoelastic responses are used to understand bond breaking
Questions? Suggestions? Remarks?
Molecular models are used to understand the linear viscoelastic response and provide design guideline
Development of a new technique for polymer melt to obtain the spectrum of relaxation times under nonlinear condition

## Slide 70
Design of an Orthogonal Superposition Rheometer
70
Loading of the cell
Bubbles
Concentricity
Problems

## Slide 71
Conclusion
71
Experimental data is in agreement with the idea of reduction
Orthogonal Superposition rheology allows to track deviations from the fluctuation - dissipation theorem
Tapez une équation ici.
But the flow cell still need to be built…
Polymeric solutions
Polydisperse systems

## Slide 72
Nonlinear Viscoelasticity : - based systems
Transient strain hardening is revealed
Stretching of the network strands :
Thermal and Force-induced dissociation

## Slide 73
Design of an Orthogonal Superposition Rheometer
73
Design of a rheometer tool placed on MCR 702e MultiDrive
Small axial
Amplitude oscillation
Large steady state
rotation
Upper shaft
Lower shaft
Flow cell
Inputs :
0.015 rev/s)
MCR 702 (SMT)

## Slide 74
Orthogonal superposition rheology
74
PnBA25k - 11Tpy – 0.75 eq.
Thermal and Force-induced dissociation
Yield strain

## Slide 75
Linear Viscoelasticity : - based systems
75
Linear response of PnBA25k - 11Tpy
Dissociation
vs
Effect of the density of ions
Effect of the nature of ions

## Slide 76
Time – Temperature Superposition (TTS) principle
76
Ref. sample
Dissociation
Thermorheological complexity
vs
Test of TTS principle
Segmental motion
PnBA25k - 7Tpy - 1eq Zn(II)
PnBA25k - 7Tpy - 1eq Zn(II)

## Slide 77
Supramolecular chemistry : Transient polymer networks
77
Dynamic and reconfigurable materials from reversible network interactions
https://www.bbau.ac.in/dept/Chemistry/TM/MCH%20301%20Superamolecular%20Chemistry%20DoC.pdf
https://olsenlab.mit.edu/research/dynamics/#:~:text=Associative%20polymers%20contain%20sticky%20groups,responsive%20and%20self%2Dhealing%20abilities.
+
: Ligand
Metal ions
« Chemistry beyond the molecule » : The supramolecular interactions
Physical bonds vs chemical bonds
How can we assess the flow dynamics
of supramolecular polymers?
Objective of the work :
Adapted from Cui et al., J. Rheol. 2022

## Slide 78
Linear Viscoelasticity : - based systems
78
Method :
Changer Magenta -> Rouse
Plate-plate geometries
Pente

## Slide 79
Linear Viscoelasticity : - based systems
79
Dissociation
vs
PnBA112k-11Tpy
PnBA112k-11Tpy

## Slide 80
Linear Viscoelasticity : - based systems
80
Method :
Emergence of a rubbery plateau
Changer Magenta -> Rouse
Formation of a dense network
Plate-plate geometries
Delay of the longest relaxation time
Pente
Slowing down of the fast relaxation
PnBA25k - 11Tpy

## Slide 81
Linear Viscoelasticity : - based systems
81
Method :
Changer Magenta -> Rouse
Plate-plate geometries
Pente
PnBA25k - 11Tpy

## Slide 82
Linear Viscoelasticity : - based systems
82
Linear response of PnBA25k - 11Tpy
M :
Dissociation
vs

## Slide 83: Focus of the research
Int
Shear rheology
Strain-controlled rheometer
83
[1] www.anton-paar.com (September, 18 2021)
[1]
Oscillatory shear rheology
Nonlinear shear rheology
Notes: Models based on the models given in class for the shear and elongational flow.
For the shear flow : the lower plate stays still while the upper one moves. So v_x(0) = 0. The flow is established so the only velocity (in 2D) is parallel to the plates and varies only along x (stationary flow, each cross section, same velocity profile).
For shear flow : 1D example shown. Velocity of center doesn’t change. The rest is strtched proportionally to the strain rate (called hecnky strain rate). Of course, since 1D, only 1 velocity component depending on one direction.
Both can be generalized in 3D.

## Slide 84
Time – Temperature Superposition (TTS) principle
84
Ref. sample
Dissociation
Thermorheological complexity
vs
Test of TTS principle
Segmental motion
PnBA25k - 7Tpy - 1eq Zn(II)
PnBA25k - 7Tpy - 1eq Zn(II)

## Slide 85
Nonlinear Viscoelasticity : - based systems
85
+
Metal Ions
(
Transient strain hardening is revealed
Stretching of the network strands :
PnBA25k – 7tpy
PnBA25k - 7Tpy – 0.75 eq.

## Slide 86
86
« Chemistry beyond the molecule » : The supramolecular interactions
Dynamic and reconfigurable materials from reversible network interactions
https://www.bbau.ac.in/dept/Chemistry/TM/MCH%20301%20Superamolecular%20Chemistry%20DoC.pdf
https://olsenlab.mit.edu/research/dynamics/#:~:text=Associative%20polymers%20contain%20sticky%20groups,responsive%20and%20self%2Dhealing%20abilities.
Rubinstein, M., and A. N. Semenov, “Dynamics of entangled solutions of associating polymers,” Macromolecules 34, 1058–1068 (2001)
Orthogonal superposition rheology

## Slide 87
Orthogonal superposition rheology
87
« Chemistry beyond the molecule » : The supramolecular interactions
Dynamic and reconfigurable materials from reversible network interactions
https://www.bbau.ac.in/dept/Chemistry/TM/MCH%20301%20Superamolecular%20Chemistry%20DoC.pdf
https://olsenlab.mit.edu/research/dynamics/#:~:text=Associative%20polymers%20contain%20sticky%20groups,responsive%20and%20self%2Dhealing%20abilities.
Rubinstein, M., and A. N. Semenov, “Dynamics of entangled solutions of associating polymers,” Macromolecules 34, 1058–1068 (2001)

## Slide 88
Conclusion
88
Yield strain

## Slide 89
Time – Temperature Superposition (TTS) principle
89
Ref. sample
Dissociation
Thermorheological complexity
vs
Test of TTS principle
Segmental motion
PnBA25k - 7Tpy - 1eq Zn(II)
PnBA25k - 7Tpy - 1eq Zn(II)

## Slide 90
Time – Temperature Superposition (TTS) principle
90
Ref. sample
Dissociation
Thermorheological complexity
vs
Test of TTS principle
Segmental motion
PnBA25k - 7Tpy - 1eq Zn(II)
PnBA25k - 7Tpy - 1eq Zn(II)

## Slide 91
Time – Temperature Superposition (TTS) principle
91
Ref. sample
Dissociation
Thermorheological complexity
vs
Test of TTS principle
Segmental motion
PnBA25k - 7Tpy - 1eq Zn(II)
PnBA25k - 7Tpy - 1eq Zn(II)

## Slide 92
Nonlinear Viscoelasticity : - based systems
92
+
Metal Ions
(
Transient strain hardening is revealed
Stretching of the network strands :
PnBA25k – 7tpy
PnBA25k - 7Tpy – 0.75 eq.

## Slide 93
Orthogonal superposition rheology
93
PnBA25k - 11Tpy – 0.75 eq.
Thermal and Force-induced dissociation
Yield strain

## Slide 94
Supramolecular chemistry : Transient polymer networks
94
Dynamic and reconfigurable materials from reversible network interactions
https://www.bbau.ac.in/dept/Chemistry/TM/MCH%20301%20Superamolecular%20Chemistry%20DoC.pdf
https://olsenlab.mit.edu/research/dynamics/#:~:text=Associative%20polymers%20contain%20sticky%20groups,responsive%20and%20self%2Dhealing%20abilities.
+
: Ligand
Metal ions
« Chemistry beyond the molecule » : The supramolecular interactions
Physical bonds vs chemical bonds
How can we tune the flow dynamics
of supramolecular polymers?
Objective of the work :
Adapted from Cui et al., J. Rheol. 2022

## Slide 95: Outline
Material of interest
M :
Lability
Terpyridine-modified poly(n-butyl acrylate)
Characteristics of the samples
Gelation by metal-ligand complexation
Measured via a) GPC b) NMR c) DSC
Sample | [kg/mol]a |  | Functional groups/chainb | 
PnBA25k-7Tpy | 25 | - | 7 | -52.1
PnBA25k-11Tpy | 25 | - | 11 | -47.2
PnBA112k-11Tpy | 139 | 7.7 | 13 | -42.1
Sample |  |  | Functional groups/chainb | 
PnBA25k-7Tpy | 25 | - | 7 | -52.1
PnBA25k-11Tpy | 25 | - | 11 | -47.2
PnBA112k-11Tpy | 139 | 7.7 | 13 | -42.1

## Slide 96
Linear Viscoelasticity : - based systems
96
Method :
Emergence of a rubbery plateau
Changer Magenta -> Rouse
Formation of a dense network
Plate-plate geometries
Delay of the longest relaxation time
Pente
Slowing down of the fast relaxation
PnBA25k - 11Tpy

## Slide 97
Time – Temperature Superposition (TTS) principle
97
Ref. sample
Dissociation
Thermorheological complexity
vs
Test of TTS principle
Segmental motion
PnBA25k - 7Tpy - 1eq Zn(II)
PnBA25k - 7Tpy - 1eq Zn(II)

## Slide 98
Pseudo-Mastercurves via TTS principle
For
For
98
Building pseudo-mastercurves
PnBA25k - 7Tpy - 1eq Zn(II)
PnBA25k - 7Tpy - 1eq Zn(II)
(see Zhang et al., Macromol. 2016)

## Slide 99
Linear Viscoelasticity : - based systems
99
Linear response of PnBA25k - 11Tpy
as per rubber elasticity theory
Extra-elasticity
Extra-elasticity ?
- Aggregates
- Chain stretch
Fits

## Slide 100
Linear Viscoelasticity : - based systems
Association time :
Zhang et al., Macromol. 2016
]
 | 1 eq. | 0.75 eq. | 0.5 eq. | 0.25 eq. | 0.125 eq.
Tpy 11 | 81.4 | 67.6 | 61.5 | 36.9 | 36.4
Tpy 7 | 51.2 | 49.4 | - | - | -
100
Shifts of PnBA25k - 11Tpy

## Slide 101
Linear Viscoelasticity : - based systems
101
PnBA25k - 11Tpy – 0.5 eq(II)
Presence of ordered aggregates ?
0.5 eq
0.5 eq
PnBA25k - 11Tpy

## Slide 102: Outline
Linear Viscoelasticity : Entangled systems
Ions
Effect of the density of ions
0.5 eq.
Stoechiometric amount
Excess
Deficiency
102
PnBA112k-11Tpy
PnBA112k-11Tpy
Fitted using a home-made sticky reptation model

## Slide 103: Outline
Linear Viscoelasticity : Entangled systems
103
1.25 eq.
2.5 eq.
Semenov, A. N., & Rubinstein, M. Macromolecules 2002, 35(12), 4821–4837.
PnBA112k-11Tpy
is much more labile than
Fitted using a home-made sticky reptation model
PnBA112k-11Tpy
PnBA112k-11Tpy
Increase of at high [

## Slide 104
Linear Viscoelasticity : Entangled systems
1.25 eq.
2.5 eq.
(Reptation motion)
3 temperature dependences :
vs
Segmental motion
vs
Hopping of the aggregates
Motion of the center of mass
(see for physics : Semenov & Rubinstein, Macromolecules, 2002)
PnBA112k-11Tpy
PnBA112k-11Tpy
104

## Slide 105
Steady shear measurements : Method
105
Plate-plate geometries
Cone-partitioned-plate geometries
Cone-Partitioned-Plate geometry (CPP)
Cone geometry
Polymer sample
Outer hollowed parallel plate
Inner parallel plate
Translation stages for alignement
Nonlinear shear rheology techniques for polymer melt
Upper flat plate
(Reproduced from : Costanzo et al., Macromolecules, 2016)
(see for physics : Semenov & Rubinstein, Macromolecules, 2002)

## Slide 106
Steady shear measurements : Method
106
Cone geometry
Polymer sample
Outer hollowed parallel plate
Inner parallel plate
Translation stages for alignement
Inward propagation of edge fracture
CPP measures only the inner part
Plate-plate geometries
Cone-partitioned-plate geometries
Upper flat plate
Cone-Partitioned-Plate geometry (CPP)
Nonlinear shear rheology techniques for polymer melt
(Reproduced from : Costanzo et al., Macromolecules, 2016)

## Slide 107
Nonlinear Viscoelasticity : - based systems
107
+
Metal Ions
(
Transient strain hardening is revealed
Stretching of the network strands :
PnBA25k – 7tpy
PnBA25k - 7Tpy – 0.75 eq.

## Slide 108
Nonlinear Viscoelasticity : - based systems
108
PnBA25k - 11Tpy – 0.75 eq.
Thermal and Force-induced dissociation
Yield strain

## Slide 109
Nonlinear Viscoelasticity : - based systems
109
PnBA25k - 11Tpy – 0.75 eq.
Thermal and Force-induced dissociation
Yield strain

## Slide 110
Nonlinear Viscoelasticity : - based systems
110
Effects of the temperature
PnBA25k - 12Tpy – 0.75 eq.
TTS principle

## Slide 111
Nonlinear Viscoelasticity : - based systems
111
Violation of Cox-Merz rule for associative polymers
Flow curve
PnBA25k - 11Tpy
PnBA25k - 7Tpy
References shown at

## Slide 112
Conclusion
112
Sticky Reptation model with a “delayed CLF” fits the data well in the Rouse and the terminal regime but is less successful in the rubbery plateau
Playing on the density and the nature of ions allows to tune and
Associative systems exhibit well the separation of the timescales predicted by the theory
Sticky Rouse model fits well unentangled associative in the Rouse
SAXS
Detect the presence of aggregates
More characterization methods are needed
Nonlinear data shows transient shear hardening, constant yield strain and TTS
Questions? Suggestions? Remarks?
But a structure develops at high …

## Slide 113
Conclusion
113
Thank you for you attention !
Questions, suggestions ?

## Slide 114
Supramolecular chemistry : Transient polymer networks
114
« Chemistry beyond the molecule » : The supramolecular interactions
Stimuli responsive
Self-healing properties
High tunability (Stiffness, Toughness & Relaxation time)
Formation of a dynamic and reversible polymeric network
Dynamic and reconfigurable materials from reversible network interactions
https://www.bbau.ac.in/dept/Chemistry/TM/MCH%20301%20Superamolecular%20Chemistry%20DoC.pdf
https://olsenlab.mit.edu/research/dynamics/#:~:text=Associative%20polymers%20contain%20sticky%20groups,responsive%20and%20self%2Dhealing%20abilities.
Properties :
Physical bonds vs chemical bonds
Rubinstein, M., and A. N. Semenov, “Dynamics of entangled solutions of associating polymers,” Macromolecules 34, 1058–1068 (2001)
…
(see for example : Seiffert . Adv. Polym. Sci. 2015, 268, 288.)
Cui, K., and J. P. Gong, J. Rheol. 66, 1093 (2022)

## Slide 115
Supramolecular chemistry : Transient polymer networks
115
Dynamic and reconfigurable materials from reversible network interactions
https://www.bbau.ac.in/dept/Chemistry/TM/MCH%20301%20Superamolecular%20Chemistry%20DoC.pdf
https://olsenlab.mit.edu/research/dynamics/#:~:text=Associative%20polymers%20contain%20sticky%20groups,responsive%20and%20self%2Dhealing%20abilities.
Cui, K., and J. P. Gong, J. Rheol. 66, 1093 (2022)
+
: Ligand
Metal ions
« Chemistry beyond the molecule » : The supramolecular interactions
In the nature…
Harrington, M. J. et al., Science, 328(5975), 216–220 (2010)
Physical bonds vs chemical bonds

## Slide 116
Supramolecular chemistry : Transient polymer networks
116
« Chemistry beyond the molecule » : The supramolecular interactions
Formation of a dynamic and reversible polymeric network
Dynamic and reconfigurable materials from reversible network interactions
https://www.bbau.ac.in/dept/Chemistry/TM/MCH%20301%20Superamolecular%20Chemistry%20DoC.pdf
https://olsenlab.mit.edu/research/dynamics/#:~:text=Associative%20polymers%20contain%20sticky%20groups,responsive%20and%20self%2Dhealing%20abilities.
Applications :
Physical bonds vs chemical bonds
Rubinstein, M., and A. N. Semenov, “Dynamics of entangled solutions of associating polymers,” Macromolecules 34, 1058–1068 (2001)
(see for example : Seiffert . Adv. Polym. Sci. 2015, 268, 288.)
Adapted from Cui, K., and J. P. Gong, J. Rheol. 66, 1093 (2022)
Self-healing properties
Self healing properties

## Slide 117
Conclusion
117
PnBA25k – 12tpy

## Slide 118
The Sticky Rouse model
The Rouse process
The Sticky Rouse process
Delay
118

## Slide 119: Outline
The Sticky reptation model
Case
Case
119
Leibler, L., Rubinstein, M., & Colby, R. H. Macromolecules 1991, 24(16), 4701–4707.
Chen, Q., Zhang, Z., & Colby, R. H. Journal of Rheology 2016, 60(6), 1031–1040.
Chen et al., J Rheol. 2016
Leibler et al., Macromol. 1991

## Slide 120: Outline
The Sticky reptation model
120
Analogy with an entangled polymer
Leibler, L., Rubinstein, M., & Colby, R. H. Macromolecules 1991, 24(16), 4701–4707.
Tube with a lifetime
Chen et al., J Rheol. 2016
Leibler et al., Macromol. 1991
Leibler, L., Rubinstein, M., & Colby, R. H. Macromolecules 1991, 24(16), 4701–4707.
Chen, Q., Zhang, Z., & Colby, R. H. Journal of Rheology 2016, 60(6), 1031–1040.

## Slide 121
Material of interest
121
Elaboration of a metallo-supramolecular bulk polymer (MSBP)
Free flowing polymeric solution
Free standing organo-gel
Bulk solidsoft elastic
Chloride
(ZnCl , CuCl ,NiCl ,…)
2
2
2
Solvent
removal
Dilution at high concentration (400 g/l)

## Slide 122
Linear Viscoelasticity : - based systems
122
Hardening
PnBA25k - 12Tpy – 0.5 eq
Introduction of leads to the formation of a structure…

## Slide 123
Linear Viscoelasticity : - based systems
123
Method :
Emergence of a rubbery plateau
Changer Magenta -> Rouse
Formation of a dense network
Plate-plate geometries
Delay of the longest relaxation time
Pente
Slowing down of the fast relaxation
PnBA27k - 12Tpy

## Slide 124
Nonlinear Viscoelasticity : - based systems
124
PnBA25k - 12Tpy – 0.75 eq.
Thermal and Force-induced dissociation
Constant yield strain
Yield strain

## Slide 125
Supramolecular chemistry : Transient polymer networks
125
« Chemistry beyond the molecule » : The supramolecular interactions
Stimuli responsive
Self-healing properties
High tunability (Stiffness, Toughness & Relaxation time)
Formation of a dynamic and reversible polymeric network
Dynamic and reconfigurable materials from reversible network interactions
https://www.bbau.ac.in/dept/Chemistry/TM/MCH%20301%20Superamolecular%20Chemistry%20DoC.pdf
https://olsenlab.mit.edu/research/dynamics/#:~:text=Associative%20polymers%20contain%20sticky%20groups,responsive%20and%20self%2Dhealing%20abilities.
Properties :
Physical bonds vs chemical bonds
Cui, K., and J. P. Gong, J. Rheol. 66, 1093 (2022)
Zhuge, F.; Hawke, L. G. D.; Fustin, C.-A.; Gohy, J.-F.; van Ruymbeke, E. Decoding the linear viscoelastic properties of model telechelic metallo-supramolecular polymers. J. Rheol. 2017, 61(6), 1245–1262.
Rubinstein, M., and A. N. Semenov, “Dynamics of entangled solutions of associating polymers,” Macromolecules 34, 1058–1068 (2001)
…

## Slide 126
Time – Temperature superposition principle
126
Ref. sample
1eq Zn(II) sample
Horizontal shift factors :
Horizontal shift factors :
1eq Zn(II) sample

## Slide 127
Time – Temperature superposition principle
127
Ref. sample
1eq Zn(II) sample
Horizontal shift factors :
Horizontal shift factors :
1eq Zn(II) sample

## Slide 128
Time – Temperature superposition principle
128
Ref. sample
1eq Zn(II) sample
Horizontal shift factors :
Horizontal shift factors :
1eq Zn(II) sample

## Slide 129
Linear Viscoelasticity : - based systems
129
Association time :
Zhang et al., Macromol. 2016
Lyons et al.
40 kJ/mol

## Slide 130
Linear Viscoelasticity : - based systems
130
Association time :
Zhang et al., Macromol. 2016
Lyons et al.
40 kJ/mol

## Slide 131
Nonlinear Viscoelasticity : - based systems
131
Stress-strain curve reveals yield strain
PnBA25k - 12Tpy – 0.75 eq.
PnBA25k – 7tpy
Thermal bond dissociation
Force – induced dissociation
Force-induced bond dissociation

## Slide 132
Nonlinear Viscoelasticity : - based systems
132
Stress-strain curve reveals yield strain
PnBA25k - 12Tpy – 0.75 eq.
Thermal bond dissociation
Force – induced dissociation

## Slide 133
Nonlinear shear viscosity
133
Effects of the temperature
vs
43.46
7.042
24.48
3.967
1.252
13.75
0.7042
7.729
0.397
4.346
vs
vs
vs
vs
vs
TTS principle

## Slide 134
134
Horizontal shift factors
Association time :
Linear Viscoelasticity : - based systems

## Slide 135
Linear Viscoelasticity : - based systems
135

## Slide 136
General objective
136
Molecular structure
(Entanglements and interchain bonds)
Viscoelastic properties
Tailored polymers
Molecular modelling

## Slide 137: Outline
Materials : Entangled systems
Eq. |  | 
0.25 | X | 
0.5 | X | X
0.75 | X | X
1.5 | X | X
2.5 |  | X
Eq. |  | 
0.25 | X | 
0.5 | X | X
0.75 | X | X
1.5 | X | X
2.5 |  | X
kg/mol
M :
Lability
TPA’s/chain =
PDI
Terpyridine-modified poly(n-butyl acrylate)

## Slide 138
Material of interest
138
Sample | [kg/mol] | Ð |  | Functional groups/chain | 
PnBA27k-7Tpy | 25 | 1.18 | - | 7 | 2.2
PnBA27k-12Tpy | 25 | 1.21 | - | 11 | 
PnBA27k-11Tpy | 112 | 1.2 | 7.5 | 11 | 
Sample |  | Ð |  | Functional groups/chain | 
PnBA27k-7Tpy | 25 | 1.18 | - | 7 | 2.2
PnBA27k-12Tpy | 25 | 1.21 | - | 11 | 
PnBA27k-11Tpy | 112 | 1.2 | 7.5 | 11 | 
Terpyridine
+
n-Butyl Acrylate (nBA)
Terpyridine acrylate (TPA)
Characteristics of the samples
High binding affinity
Rich coordination chemistry
Thermal stability (
Poly(n-butyl acrylate)
Amorphous & low
Thermal stability (
Mildly flexible
:
Poly(n-butyl acrylate)-co- Poly(terpyridine acrylate)

## Slide 139
The Sticky Rouse model
139
Horizontal shift factors :
Horizontal shift factors :
1eq Zn(II) sample

## Slide 140
Horizontal shift factors :
WLF equation :
K
140
Free volume correction :
Wagner, Rheol. Acta, 2014
Wagner, M. H. Rheologica Acta 2014, 53(10-11), 765–777.
Time – Temperature superposition principle
PBU8

## Slide 141
Linear Viscoelasticity
141
+
n-Butyl Acrylate (nBA)
Terpyridine acrylate (TPA)
PnBA-co-TPA
Delay

## Slide 142
Supramolecular chemistry : Transient polymer networks
142
« Chemistry beyond the molecule » : The supramolecular interactions
Dynamic and reconfigurable materials from reversible network interactions
https://www.bbau.ac.in/dept/Chemistry/TM/MCH%20301%20Superamolecular%20Chemistry%20DoC.pdf
https://olsenlab.mit.edu/research/dynamics/#:~:text=Associative%20polymers%20contain%20sticky%20groups,responsive%20and%20self%2Dhealing%20abilities.
Physical bonds vs chemical bonds
Cui, K., and J. P. Gong, J. Rheol. 66, 1093 (2022)
Zhuge, F.; Hawke, L. G. D.; Fustin, C.-A.; Gohy, J.-F.; van Ruymbeke, E. Decoding the linear viscoelastic properties of model telechelic metallo-supramolecular polymers. J. Rheol. 2017, 61(6), 1245–1262.
Rubinstein, M., and A. N. Semenov, “Dynamics of entangled solutions of associating polymers,” Macromolecules 34, 1058–1068 (2001)
+
: Ligand
Metal ions
Schematic reaction scheme

## Slide 143
Supramolecular chemistry : Reversible networks
143
Wiley Interdiscip. Rev. Nanomed. Nanobiotechnol. 2013, 5, 582−612.
« Chemistry beyond the molecule » : The supramolecular interactions
- Stimuli responsive
- Self-healing properties
- Self-healing properties

## Slide 144
Supramolecular chemistry
144
Summary of supramolecular interactions
Wiley Interdiscip. Rev. Nanomed. Nanobiotechnol. 2013, 5, 582−612.
+
: Ligand
Metal ions
Elementary reactions
Formation of a dynamic and reversible network

## Slide 145
Supramolecular chemistry : Reversible networks
145
Summary of supramolecular interactions
Wiley Interdiscip. Rev. Nanomed. Nanobiotechnol. 2013, 5, 582−612.

## Slide 146
Material of interest
146
In the LVE regime, dissociation of crosslinks results in flow
Unentangled chains
Unentangled associative chains
Delay

## Slide 147
Material of interest
147
In the LVE regime, dissociation of crosslinks results in flow
Unentangled chains
Delay
Bead

## Slide 148
The Sticky Rouse model
The Rouse process
The Sticky Rouse process
Delay
148
Chen, Q.; Huang, C.; Weiss, R. A.; Colby, R. H. Macromolecules 2015, 48 (4), 1221–1230.
Baxandall, Macromol. 1989
Baxandall, L. G. Macromolecules 1989, 22 (4), 1982–1988.

## Slide 149
The Sticky Rouse model
149
WLF equation :

## Slide 150
Nonlinear shear viscosity
150
PnBA25k - 7Tpy – 1 eq.
PnBA25k – 7tpy
+
Metal Ions
(
Transient shear hardening !

## Slide 151
Unentangled sticky chains
151
+
n-Butyl Acrylate (nBA)
Terpyridine acrylate (TPA)
PnBA-co-TPA

## Slide 152
Materials : Unentangled systems
152
+
Metal Ions
(
Metallo-supramolecular
Network
=
+
n-Butyl Acrylate (nBA)
Terpyridine acrylate (TPA)
PnBA-co-TPA
Characteristics of the sample
Cone-Partitioned-Plate geometry (CPP)
Snijkers & Vlassopoulos, J. Rheol. 2011
Nonlinear shear measurements
Sample | [kg/mol] | Ð | Functional groups/chain | /Tpy ratio | 
PnBA27k-7Tpy | 25 | 1.18 | 7 | : 0/0.75/1 eq. | 2.2
PnBA27k-12Tpy | 25 | 1.21 | 11 | : 0.25/0.5/0.75/1 eq. : 0.25/0.5 eq/1 eq. | 
Sample |  | Ð | Functional groups/chain |  | 
PnBA27k-7Tpy | 25 | 1.18 | 7 |  | 2.2
PnBA27k-12Tpy | 25 | 1.21 | 11 |  | 

## Slide 153
Outline
153
1. Unentangled associative polymers
2. Entangled associative polymers
based on H-bond
based on metal-ligand coordination

## Slide 154
Materials : Unentangled systems
 | [kg/mol] | Upy’s/chain
PB - UPy | 4.5 | 2.2
 | 5.1 | 4
 | 5.1 | 5.3
 | 4.9 | 8.2
 |  | Upy’s/chain
PB - UPy | 4.5 | 2.2
 | 5.1 | 4
 | 5.1 | 5.3
 | 4.9 | 8.2
1,2-polybutadiene - co - ureidopyrimidinone
PB-co-UPy
Prevents stacking
154
(via NMR)

## Slide 155
The Sticky Rouse model
The Rouse process
The Sticky Rouse process
Delay
155
Chen, Q.; Huang, C.; Weiss, R. A.; Colby, R. H. Macromolecules 2015, 48 (4), 1221–1230.
Baxandall, Macromol. 1989
Baxandall, L. G. Macromolecules 1989, 22 (4), 1982–1988.

## Slide 156
Linear Viscoelasticity
Delay
PBU4
PBU6
PBU8
PBU13
156

## Slide 157
Horizontal shift factors :
WLF equation :
K
157
Free volume correction :
Wagner, Rheol. Acta, 2014
Wagner, M. H. Rheologica Acta 2014, 53(10-11), 765–777.
Time – Temperature superposition principle
PBU8

## Slide 158
Time – Temperature superposition principle
Association time :
158
Zhang, Z.; Liu, C.; Cao, X.; Gao, L.; Chen, Q. Macromolecules 2016, 49 (23), 9192–9202.
Zhang et al., Macromol. 2016
Horizontal shift factors :
PBU8
PBU8

## Slide 159
Pseudo-Mastercurves
159
With free volume correction
depends on the number of slow modes, and the lifetime of a bond
decreases with increasing which means that the number of returns should decrease with

## Slide 160
The Sticky Rouse model
160
Molar mass distribution :
Sticker distribution :
 | PBU6 | PBU8 | PBU13
[g/mol] | 1150 | 900 | 700
[s] | 0.2 | 0.22 | 1.2
[s] |  |  | 
 | PBU6 | PBU8 | PBU13
 | 1150 | 900 | 700
 | 0.2 | 0.22 | 1.2
Fitting Parameters
PBU6
PBU8
PBU13

## Slide 161: Outline
Materials : Entangled systems
Eq. |  | 
0.25 | X | 
0.5 | X | X
0.75 | X | X
1.5 | X | X
2.5 |  | X
Eq. |  | 
0.25 | X | 
0.5 | X | X
0.75 | X | X
1.5 | X | X
2.5 |  | X
kg/mol
M :
Lability
TPA’s/chain =
PDI
Terpyridine-modified poly(n-butyl acrylate)

## Slide 162: Outline
The Sticky reptation model
Case
Case
162
Leibler, L., Rubinstein, M., & Colby, R. H. Macromolecules 1991, 24(16), 4701–4707.
Chen, Q., Zhang, Z., & Colby, R. H. Journal of Rheology 2016, 60(6), 1031–1040.
Chen et al., J Rheol. 2016
Leibler et al., Macromol. 1991

## Slide 163: Outline
The Sticky reptation model
163
Analogy with an entangled polymer
Leibler, L., Rubinstein, M., & Colby, R. H. Macromolecules 1991, 24(16), 4701–4707.
Tube with a lifetime
Chen et al., J Rheol. 2016
Leibler et al., Macromol. 1991
Leibler, L., Rubinstein, M., & Colby, R. H. Macromolecules 1991, 24(16), 4701–4707.
Chen, Q., Zhang, Z., & Colby, R. H. Journal of Rheology 2016, 60(6), 1031–1040.

## Slide 164: Outline
Time – Temperature superposition principle
27.2 | 52.1
27.2 | 52.1
kJ/mol
,
164

## Slide 165: Outline
Linear Viscoelasticity
Ions
Effect of the density of ions
0.5 eq.
Stoechiometric amount
Excess
Deficiency
165

## Slide 166: Outline
Linear Viscoelasticity
Effect of the density of ions
166
1.25 eq. Cu
2.5 eq. Cu
Presence of aggregates in the system
Hopping of an aggregate
Reptation of the chains
Semenov, A. N., & Rubinstein, M. Macromolecules 2002, 35(12), 4821–4837.
No formation of mono-complex

## Slide 167: Outline
Linear Viscoelasticity
Effect of the nature of the ions
167
is much more labile than
[s] | [s] | [s]
1 | 75 | 5000
1 | 75 | 5000
Relaxation times

## Slide 168
Modelling
1. Rouse Regime
2. Sticky Rouse Regime
3. Sticky Reptation (Time-Marching Algorithm)
with
and
Van Ruymbeke, E., Bailly, C., Keunings, R., & Vlassopoulos, D. (2006). Macromolecules, 39(18), 6248–6259.
Van Ruymbeke et al., Macromol. 2006

## Slide 169
Modelling
1. Rouse Regime
2. Sticky Rouse Regime
3. Sticky Reptation (Time-Marching Algorithm)
with
and
169
Van Ruymbeke, E., Bailly, C., Keunings, R., & Vlassopoulos, D. (2006). Macromolecules, 39(18), 6248–6259.
Van Ruymbeke et al., Macromol. 2006

## Slide 170
Modelling
1. Rouse Regime
2. Sticky Rouse Regime
3. Sticky Reptation (Time-Marching Algorithm)
with
and
170
Van Ruymbeke, E., Bailly, C., Keunings, R., & Vlassopoulos, D. (2006). Macromolecules, 39(18), 6248–6259.
Van Ruymbeke et al., Macromol. 2006

## Slide 171
Modelling
1. Rouse Regime
2. Sticky Rouse Regime
with
and
171
Van Ruymbeke, E., Bailly, C., Keunings, R., & Vlassopoulos, D. (2006). Macromolecules, 39(18), 6248–6259.
3. Sticky Reptation (Time-Marching Algorithm)
Van Ruymbeke et al., Macromol. 2006

## Slide 172
Modelling
1. Rouse Regime
2. Sticky Rouse Regime
with
and
172
Van Ruymbeke, E., Bailly, C., Keunings, R., & Vlassopoulos, D. (2006). Macromolecules, 39(18), 6248–6259.
3. Sticky Reptation (Time-Marching Algorithm)
Van Ruymbeke et al., Macromol. 2006

## Slide 173: Modelling: Contour Length Fluctuation
Average duration of a « k-strand »
X
X
X
X
X
X
X
Probability of a « k-strand » :
Probability to be open = pfree
Average waiting time for seeing a « k-strand » :
173
Notes: Models based on the models given in class for the shear and elongational flow.
For the shear flow : the lower plate stays still while the upper one moves. So v_x(0) = 0. The flow is established so the only velocity (in 2D) is parallel to the plates and varies only along x (stationary flow, each cross section, same velocity profile).
For shear flow : 1D example shown. Velocity of center doesn’t change. The rest is strtched proportionally to the strain rate (called hecnky strain rate). Of course, since 1D, only 1 velocity component depending on one direction.
Both can be generalized in 3D.

## Slide 174: Sticky reptation
When the lifetime of a « k-strand » > the diffusion time of a « k-strand », CLF stops
(In case of early fluctuations)
Hypothesis :
« Stepwise CLF »
« Sticky » CLF
CLF
Notes: Models based on the models given in class for the shear and elongational flow.
For the shear flow : the lower plate stays still while the upper one moves. So v_x(0) = 0. The flow is established so the only velocity (in 2D) is parallel to the plates and varies only along x (stationary flow, each cross section, same velocity profile).
For shear flow : 1D example shown. Velocity of center doesn’t change. The rest is strtched proportionally to the strain rate (called hecnky strain rate). Of course, since 1D, only 1 velocity component depending on one direction.
Both can be generalized in 3D.

## Slide 175: Modelling: Contour Length Fluctuation
175
0.5 eq. Zn
0.75 eq. Zn
0.25 eq. Zn
0.5 eq. Cu
Reference
Notes: Models based on the models given in class for the shear and elongational flow.
For the shear flow : the lower plate stays still while the upper one moves. So v_x(0) = 0. The flow is established so the only velocity (in 2D) is parallel to the plates and varies only along x (stationary flow, each cross section, same velocity profile).
For shear flow : 1D example shown. Velocity of center doesn’t change. The rest is strtched proportionally to the strain rate (called hecnky strain rate). Of course, since 1D, only 1 velocity component depending on one direction.
Both can be generalized in 3D.

## Slide 176
Conclusion
176
Sticky Reptation model with a “delayed CLF” fits the data well in the Rouse and the terminal regime but is less successful in the rubbery plateau
By playing on the density and the nature of ions, and the magnitude of the plateau of metallo-supramolecular systems can be tuned
Both systems exhibit the separation of the timescales () predicted by the theory
Sticky Rouse model fits well unentangled associative in the Rouse

## Slide 177
Conclusion
177
Thank you for you attention !

## Slide 178: Comparison
Int
178
Tube-segment occupation function
(Reptation + CLF)
Notes: Models based on the models given in class for the shear and elongational flow.
For the shear flow : the lower plate stays still while the upper one moves. So v_x(0) = 0. The flow is established so the only velocity (in 2D) is parallel to the plates and varies only along x (stationary flow, each cross section, same velocity profile).
For shear flow : 1D example shown. Velocity of center doesn’t change. The rest is strtched proportionally to the strain rate (called hecnky strain rate). Of course, since 1D, only 1 velocity component depending on one direction.
Both can be generalized in 3D.

## Slide 179: Sticky reptation
Int
X
X
X
X
X
X
X
X
X
X
X
X
X
X
X
Associated sticker
Unassociated sticker
X
X
X
X
X
X
X
At equilibrium :
-
X
X
-
Lifetime of a free sticker
Lifetime of a closed sticker
Notes: Models based on the models given in class for the shear and elongational flow.
For the shear flow : the lower plate stays still while the upper one moves. So v_x(0) = 0. The flow is established so the only velocity (in 2D) is parallel to the plates and varies only along x (stationary flow, each cross section, same velocity profile).
For shear flow : 1D example shown. Velocity of center doesn’t change. The rest is strtched proportionally to the strain rate (called hecnky strain rate). Of course, since 1D, only 1 velocity component depending on one direction.
Both can be generalized in 3D.

## Slide 180
Longitudinal modes
X
X
0
X
0
X
X
X
X
X
0
X
X
0
X
Associated sticker
Entanglements
0
t < :
0
X
X
0
X
X
t :
Unassociated sticker
X
0
X
X
0
X
0
X
X
0
X
0
X
X
0
X
X
0
0
X
X
0
X
X
0