Selection and characterization of ionic liquids for the potential recovery of dimethyl carbonate from methanol/dimethyl carbonate by pervaporation

Xiao Xu a, b, Cristhian Molina Fernandez a, b, Patricia Luis a, b*

a Materials & Process Engineering (iMMC-IMAP), UCLouvain, Place Sainte Barbe 2, 1348 Louvain-la-Neuve, Belgium

b Research & Innovation Centre for Process Engineering (ReCIPE), Place Sainte Barbe, 2 bte L5.02.02 - B-1348 Louvain-la-Neuve (Belgium)

The use of pervaporation to separate organic-organic mixtures has attracted increasing interest in the research community, as the technology exhibits great potential (considering its low energy consumption) [1]. For example, valorisation of CO2 as a platform molecule to produce dimethyl carbonate (DMC) is of utmost interest, but it involves the reaction of CO2 with methanol (MeOH) to produce DMC [2-4]. This reaction is limited by the equilibrium and an azeotrope between dimethyl carbonate and methanol is also present. Thus, the low yield and high separation costs using conventional technology make this process uninteresting for a real application.

In the past few years, ionic liquids (ILs) have received more and more attention as catalysts for the synthesis of DMC from CO2 and MeOH, considering their wide liquid range and excellent thermal and chemical stability[5]. Besides being used as catalysts, ILs have also showed potential in pervaporation separation. In order to screen out ILs suitable for extracting dimethyl carbonate (DMC) from a mixture of DMC/methanol (MeOH), three kinds of ionic liquids (ILs) 1-Octyl-3-methylimidazolium bromide [1O3MIm][Br], 1-Octyl-1,4-diazabicyclo[2.2.2]octanium bromide [ODABCO][Br], and 1-Octyl-3-methylimidazolium bis(trifluoromethanesulfonyl)imide [1O3MIm][Br] were successfully synthesized and their chemical structures were confirmed by NMR. These three ILs and one commercial IL Tetrabutylammonium bromide [TBA][Br] were further characterised by DSC/TGA and processed into supported ionic liquid membranes (SILMs). SILMs shows a decrease in MeOH permeance almost without compromising DMC permeance and higher ideal DMC/MeOH selectivity at low temperature compared to PAN.

Keywords: Ionic liquids; Pervaporation; Dimethyl carbonate; Methanol

*Corresponding author: Prof. Patricia Luis, patricia.luis@uclouvain.be, 010/47.24.02

References

1.	Xu, X., et al., MOF-based membranes for pervaporation. Separation and Purification Technology, 2021: p. 119233.

2.	Li, W., et al., Supported ionic liquid membranes for the separation of methanol/dimethyl carbonate mixtures by pervaporation. Journal of Membrane Science, 2020. 598: p. 117790.

3.	Li, W., et al., Application of pervaporation in the bio-production of glycerol carbonate. Chemical Engineering and Processing-Process Intensification, 2018. 132: p. 127-136.

4.	Tamboli, A.H., A.A. Chaugule, and H. Kim, Catalytic developments in the direct dimethyl carbonate synthesis from carbon dioxide and methanol. Chemical Engineering Journal, 2017. 323: p. 530-544.

5.	Chaugule, A.A., A.H. Tamboli, and H. Kim, Ionic liquid as a catalyst for utilization of carbon dioxide to production of linear and cyclic carbonate. Fuel, 2017. 200: p. 316-332.

Presenting author details:

Full name: Xiao Xu

Email: xiao.xu@uclouvain.be

Contact number: 010/47.92.09

Affiliation: Institute of Mechanics, Materials and Civil Engineering, Université catholique de Louvain

Topic: reactive pervaporation

Other questions:

- Are you a PhD student or an Early-Career Researcher (ECR) *?

PhD student

- Would you like to be considered for oral presentation (5 min for PhD student and 15 min for ECR)?

Yes

- Would you like to be considered for a presentation award (PhD student and ECR only)? Yes