## Slide 1: The GW-method approaches for molecules and automatization for solids
M.J. van Setten
Institute of Condensed Matter and Nanosciences, Université catholique de Louvain, Belgium

## Slide 4: Computational approaches
Density functional theory
  Maps the many particle problem into a single particle problem
  Scalar effective potential Vxc(r)
  Applicable to large systems: > 2000 atoms
  Broadly used across many fields of sciences
  Description of electronic levels (charge transfer), long range interactions, no proper fundamental band gaps
GW-method
  Replace the potential by a self-energy matrix: Vxc(r) → Σ(r,r’,E)
  Becoming increasingly available for bulk solids
  Significantly improved description of electronic levels (charge transfer), long range interactions, and band gaps
Notes: Improved experimental conditions

## Slide 5: GW for solids: Bandgaps
VAN SCHILFGAARDE PRL 96, 226402 (2006)
HEDIN J PHYS, COND MAT. 11 R489 (SHIRLEY)

## Slide 6: scGW for solids: Bandgaps
KRESSE PRB 75, 235102
VAN SCHILFGAARDE PRL 96, 226402 (2006)

## Slide 7: GW + BSE for solids: optical excitations
ONIDA, Rev Mod Phys 74, 601
VAN SETTEN PRB 83, 035422
NaH
Silicon
G0W0 + RPA
DFT + RPA
Exp
G0W0 + BSE

## Slide 8: GW

## Slide 9: KS v.s. Quasi-Particle equation
Electron density parameterized by KS single particle states
HEDIN Phys Rev 139, A796, HYBERTSEN and LOUIE PRB 34, 5390
Notes: At this point all is exact, now we need a way to calculate Sigma

## Slide 10: KS v.s. Quasi-Particle equation
Greens function obeying the Dyson equation
In spectral representation, expressed in terms of quasi-particle states leads to the quasi particle equation:
HEDIN Phys Rev 139, A796, HYBERTSEN and LOUIE PRB 34, 5390

## Slide 11: KS v.s. Quasi-Particle equation
Electron density parameterized by KS single particle states
Greens function in spectral representation, expressed in terms of quasi-particle states leads to the quasi particle equation:
The quasi-particle energies are the electron removal and addition energies
HEDIN Phys Rev 139, A796, HYBERTSEN and LOUIE PRB 34, 5390
Notes: At this point all is exact, now we need a way to calculate Sigma

## Slide 12: KS v.s. Quasi-Particle equation
Electron density parameterized by KS single particle states
Greens function in spectral representation, expressed in terms of quasi-particle states leads to the quasi particle equation:
The quasi-particle energies are the electron removal and addition energies
Vxc: exchange correlation potential
HEDIN Phys Rev 139, A796, HYBERTSEN and LOUIE PRB 34, 5390
Σ: self-energy
Notes: At this point all is exact, now we need a way to calculate Sigma

## Slide 13: Zeroth order quasi particle equation
Full quasi particle equation
0th order corrections (diagonal elements only)
Linearized 0th order corrections

## Slide 14: Advantages
There is a closed set of equations for the self-energy
Perturbative expansion in terms of the screened interaction in stead of the bare Coulomb interaction
The quasi-particle energies are the electron removal and addition energies
Extension to charge neutral excitations via the Bethe-Salpeter equation
Bare Coulomb interaction
Screened Coulomb interaction

## Slide 15: Hedin Equations
  Space time notation (the numbers indicate a contracted space, time and spin index)
HEDIN Phys Rev 139, A796

## Slide 16: Hedin Equations
  Space time notation (the numbers indicate a contracted space, time and spin index)
  Neglecting the second term in the vertex function leads to the GW approximation for the self-energy Fourier transformed to frequency domain:
HEDIN Phys Rev 139, A796

## Slide 17: In diagrams

## Slide 18: Molecular systems

## Slide 19: Analytic integration
Calculate the self-energy only once from KS-DFT energies and orbitals
Notes: Because of our spectral approach we can now evaluate these last experssions analitically

## Slide 20: Analytic integration
Calculate the self-energy only once from KS-DFT energies and orbitals
Spectral representation of the reducible polarization function
from TD-KS response equation
m labels excitations
Notes: Because of our spectral approach we can now evaluate these last experssions analitically

## Slide 21: Reducible response function
transition densities
Generalized Dyson equation
As used in TDHF and TDDFT
RPA or TDDFT version of the orbital rotation Hessians
For all m : Formally N6
Exploiting local basis N4

## Slide 22: G0W0 and linearized QP equation
Calculate the self-energy only once from KS-DFT energies and orbitals
Linearized 0th order Quasi-Particle equation
Notes: Because of our spectral approach we can now evaluate these last experssions analitically

## Slide 23: Matrix elements
Matrix elements to be calculated
Implemented in TURBOMOLE (escf)
Very efficient evaluation of electron-electron integrals:
  (Contracted) Gaussian basis sets
  Resolution of the Identity (RI) method
MVS, F. Weigend, F Evers
JCTC 11, 232 (2013)

## Slide 24: Plasmon pole
  Approximate the response by one single pole
  Calculate response at a few imaginary frequencies
  Analytic continuation to the real axis
  Calculate Sigma analytically
  Cheap
  Many different approaches
  Justification for complex systems

## Slide 25: Analytic continuation
  Calculate the GW integral on the imaginary axis
  Fit an n-pole expansion for Sigma in the entire complex plane
Allows for a more detailed sigma
Can be made exact
May take many poles to converge

## Slide 26: Benchmark set for molecules: GW100
Collaboration KIT Karlsruhe, FHI Berlin and Berkeley Lab US DoE
  TURBOMOLE: Gaussian basis sets, spectral representation via Casida
  FHI-Aims: numerical local orbitals, analytic continuation
  BerkeleyGW: plane waves, plasmon pole and real frequency integration
  5 different ways to evaluate the self-energy
well converged all electron reference values for IP and EA

## Slide 27: Basis-set extrapolation
SVP
TZVP
QZVP
T
Q
5

## Slide 28: Hard to converge

## Slide 29: Problems when solving the QPE
x

## Slide 30: Method agreement

## Slide 31: Some numbers
0.65 eV overestimation by plasmon pole
0.32 eV underestimation at QZVP level for the LUMO
0.12 eV underestimation at QZVP level for the HOMO
0.12 eV error by two pole analytic continuation
0.10 eV error by introducing a 150 eV cutoff on empty states and a 544 eV cutoff on the dielectric matrix
0.05 eV overestimation by RI auxiliary basis functions
0.05 eV error by introducing a 400 eV cutoff on the spectral representation of the response function

## Slide 32: Further steps

## Slide 33: Approximations within G0W0
Plasmon pole / model response
Analytic continuation / numerical integration
Neglect of semi-core state contributions / pseudo potentials

## Slide 34: Approximations within G0W0
Plasmon pole / model response
Analytic continuation / numerical integration
Neglect of semi-core state contributions / pseudo potentials
Linearized quasi particle equation (< 0.1 eV)
RI approximation (< 0.1 eV)
Difference RPA / TDDFT response (~ 0.1 eV)

## Slide 35: Approximations within G0W0
Plasmon pole / model response
Analytic continuation / numerical integration
Neglect of semi-core state contributions / pseudo potentials
Linearized quasi particle equation (< 0.1 eV)
RI approximation (< 0.1 eV)
Difference RPA / TDDFT response (~ 0.1 eV)
Off-diagonal elements
  > Perturbative correction
Neglect of self-consistency
  > Quasi-particle self-consistency
  > Partial self-consistency

## Slide 36: (partial) self-consistency
G0W0
GfoW0
GW0
foGW
qpGW
Single screening calculation
Same computational cost
Starting point independent
No off-diagonal elements

## Slide 37
qsGW
Notes: Benzene

## Slide 38
qsGW
Notes: Thiadiazole

## Slide 39
G0W0

## Slide 40
G0W0

## Slide 41
GfoW0

## Slide 42
GfoW0

## Slide 43
foGW
Notes: butene
isobuthene

## Slide 44
foGW
Notes: butene
isobuthene

## Slide 45: (partial) self-consistency
G0W0
GfoW0
GW0
foGW
qpGW
Single screening calculation
0.22 (0.07)
0.75 (0.20)
0.17 (0.03)
wrt CCSD(T)
0.43 (0.09)
@PBE
Mean Absolute Deviation (sigma2)
0.18 (0.05)
Optimized starting point
0.15 (0.02)
0.21 (0.06)
Notes: Left pbe75 right pbe0

## Slide 46: Approximations within G0W0
Plasmon pole / model response
Analytic continuation / numerical integration
Neglect of semi-core state contributions / pseudo potentials
Linearized quasi particle equation (< 0.1 eV)
RI approximation (< 0.1 eV)
Difference RPA / TDDFT response (~ 0.1 eV)
Off-diagonal elements
Self-consistency
Beyond GW …

## Slide 47: High-throughput GW
Notes: Lausanne AAS 25 mins

## Slide 48: High-throughput GW
from a structure without any human intervention to converged GW results
Automatic calculations
Screening for new compounds
Database building
Uniform results
No human bias

## Slide 49: Baby sitting
Determine optimal parallelization settings
Create input
Automatically submit jobs (to the right queue)
Monitor job status
Detect and fix errors
Restart

## Slide 50: Convergence studies
Energy cutoffs
Kpoints
Smearing
Bands
….

## Slide 51: Post processing
nscf_ebands = abiopen("si_nscf_GSR.nc").ebands
gs_ebands = abiopen("si_scf_GSR.nc").ebands
nscf_ebands.plot_with_edos(gs_ebands.get_edos())

## Slide 52: Automatically for many structures
for structure in database:
ebands_input(structure, pseudos=ONCVPSP_GGA)
for structure in database:
ebands_input(structure, pseudos=ONCVPSP_GGA)
for structure in database:
ebands_input(structure, pseudos=ONCVPSP_GGA)

## Slide 53: GW in High Throughput
‘additional’ difficulties as compared to DFT
  Pseudo potentials
  4 step calculation
  N4 scaling
  No ‘safe’ parameter set (converged results for all)
  No ‘safe’ computational settings (# cpu’s, memory, time, ...)
Notes: Pseudo potentials well tested for ground state, for gw this is not so clear ..

## Slide 54
Flow generation:
GUI or scripted
based Python package
Workflow management
ABINIT I/O
Post processing

## Slide 55
Scheduling the flow on the cluster Error handling
Convergence testing
SLURM PBSPro
Torque
SGE …

## Slide 56
Storing results: query-able entries
+ netcdf data files
(via gridfs)
Interactive analysis
and presentation of
results

## Slide 57: Automatic GW flow
On a low k-point density (2x2x2):
  Set of single parameter ground state convergence studies
  Grid of nbands X encuteps
  For each nbands find converged encuteps
  For the converged encuteps find the converged nbands
  if not found > extend grid and retest
On the final high k-point density:
  Test derivatives. (in most cases the high density derivatives turn out smaller)
  Post process (create scissor, apply scissor, plots, statistical analysis…)
(pw cutoff, …)

## Slide 58: Convergence study
On a low k-point density (2x2x2):
  Set of single parameter ground state convergence studies
  Grid of nbands X encuteps
  For each nbands find converged encuteps
  For the converged encuteps find the converged nbands
  if not found > extend grid and retest
On the final high k-point density:
  Test derivatives. (in most cases the high density derivatives turn out smaller)
  Post process (create scissor, apply scissor, plots, statistical analysis…)
(pw cutoff, …)

## Slide 59
Gold
2x2x2 kpoint mesh
14x14x14 kpoint mesh
Notes: It actually works: the shape of the surface calculated at 222 is the same as the on calculated

## Slide 60
G-G gap
(eV)

## Slide 61: Automatic GW flow
On a low k-point density (2x2x2):
  Set of single parameter ground state convergence studies
  Grid of nbands X encuteps
  For each nbands find converged encuteps
  For the converged encuteps find the converged nbands
  if not found > extend grid and retest
On the final high k-point density:
  Test derivatives. (in most cases the high density derivatives turn out smaller)
  Post process (create scissor, apply scissor, plots, statistical analysis…)
(pw cutoff, …)

## Slide 62: First application: GW160
~ 160 solids, including the not so usual suspects
Settings:
  Godby – Needs PP
  Tolerance 0.1 eV
~ 100 done at this point

## Slide 63
correlation: 0.983
R-squared: 0.966
coefficients
const: 0.4507 (0.063)
ksfgap: 1.3227 (0.028)

## Slide 65
d-states Cu, Cd

## Slide 66
d-states Cu, Cd
Heavy elements Te, Pd

## Slide 67
d-states Cu, Cd
Heavy elements Te, Pd
Experimental gaps are room temperature

## Slide 68: Some Statistics
Parameters for convergence [eV]
G0W0@PBE performance (Troom exp) [eV]

## Slide 69: Empty states v.s. Sigma cutoff

## Slide 70: Collaborators
Matteo Giantomassi
Geoffroy Hautier
Gian-Marco Rignanese
Xavier Gonze
Don Hamann
Ferdinand Kaplan
Florian Weigend
Ferdinand Evers
Fabio Caruso (FHI Berlin)
Patrick Rinke (FHI Berlin)
Sahar Sharifhades (Berkeley Lab)
Jeffey Neaton (Berkeley Lab)

## Slide 71: Pseudo Dojo
Optimized Norm Conserving Vanderbild Pseudo Potentials
  multiple projectors
  multiple gradient constraints
Don Hamann (PRB 88, 085117 (2013))
Package to facilitate PSP generation
Graphical interface
Automatized testing (6)
http://www.pseudo-dojo.org/dojo.html
Log derivatives made to agree up to 8 Ha
Notes: Multiple projectors > more degrees of freedom to fix the scattering in the empty space
Log derivatives can be made to match the all electrons ones well beyond 8 H

## Slide 72: ONCVPSP PDv0.2
Mean low cutoff 27 Ha (std 12 Ha), normal cutoff 33 Ha (std 13 Ha)
[meV]
(Comparing EOS against AE reference)

## Slide 73
Single projector PP
Carbon
log derivatives
Ghost state

## Slide 74
Single projector PP
2 projector PP
Carbon
log derivatives
Ghost state

## Slide 75: Benchmark set for molecules: GW100
Collaboration KIT Karlsruhe, FHI Berlin and Berkeley Lab US DoE
  TURBOMOLE: Gaussian basis sets, spectral representation via Casida
  FHI-Aims: numerical local orbitals, analytic continuation
  BerkeleyGW: plane waves, plasmon pole and real frequency integration
  5 different ways to evaluate the self-energy
Strictly converged all-electron reference values for IP and EA
Test PP results against all electron references for molecular systems Sternheimer GW in Abinit

## Slide 76: GW in High Throughput
‘additional’ difficulties
  Pseudo potentials
  4 step calculation
  N4 scaling
  No ‘safe’ parameter set (converged results for all)
  No ‘safe’ computational settings (# cpu’s, memory, time, ...)
DFT babysitting problem
Notes: Pseudo potentials well tested for ground state, for gw this is not so clear ..

## Slide 77: GW in High Throughput
GW babysitting problem
‘additional’ difficulties
  Pseudo potentials
  4 step calculation
  N4 scaling
  No ‘safe’ parameter set (converged results for all)
  No ‘safe’ computational settings (# cpu’s, memory, time, ...)
Notes: Pseudo potentials well tested for ground state, for gw this is not so clear ..

## Slide 78
‘additional’ difficulties
  4 step calculation
  N4 scaling
  No ‘safe’ parameter set (converged results for all)
  No ‘safe’ computational settings (# cpu’s, memory, time, ...)
  Pseudo potentials ?
GW babysitting problem
GW in High Throughput
Notes: Pseudo potentials well tested for ground state, for gw this is not so clear ..

## Slide 79: Summarizing

## Slide 80
Storing flows in a database

## Slide 81: Graphical interfaces

## Slide 82
Ipython notebook with full info: H-high.ipynb
EOS
Flows

## Slide 83: Collaborators
Florian Weigend (KIT Karlsruhe)
Ferdinand Evers (KIT Karlsruhe)
Fabio Caruso (FHI Berlin)
Patrick Rinke (FHI Berlin)
Sahar Sharifhades (Berkeley Lab)
Jeffey Neaton (Berkeley Lab)

## Slide 84: Acknowledgements
Prof. F. Evers
Dr. F. Weigend
Dipl.-Phys. F Kaplan
Center for Functional Nanostructures

## Slide 85: KS v.s. Quasi-Particle equation
Electron density parameterized by KS single particle states
Greens function in spectral representation, expressed in terms of quasi-particle states leads to the quasi particle equation:
The quasi-particle energies are the electron removal and addition energies
HEDIN Phys Rev 139, A796, HYBERTSEN and LOUIE PRB 34, 5390
Local exchange-correlation potential
Non-local energy dependent non-hermitian self-energy
Notes: At this point all is exact, now we need a way to calculate Sigma

## Slide 86: GW wrapper
Python package that wraps around the ab-initio code
Options
    What kind of GW
    Convergence tolerance
Some list of structures > ‘fully’ converged GW results

## Slide 87: 2D convergence problem

## Slide 88
Python package for:
post-processing Abinit results
generating input files automatically
creating and executing workflows (relaxations, phonons, benchmarking, convergence studies, PP testing, GW ...)
(I)Python(notebook) based tutorials
High throughput flows and high performance flows
Why python?
relatively easy to use and to learn
interactive environment (IPython, notebooks, GUIs)
excellent support for scientific applications (scipy, pandas, matplotlib...)
ecosystem
tons of other libraries

## Slide 89: DFPT

## Slide 90: Raman with frozen phonon

## Slide 91: Ecuteps ?

## Slide 92
Abipy for teaching
Different users

## Slide 94: Test results and Benchmarking
Test set including:
  H2, N2, F2, Li2, Na2, Cs2
  NH3, SiH4, SF4
  LiH, BF, CO2, H2O
  Au2, Au4
  Acetone, Acrolein, Ethylene, Isobutane
  Methane – Butane, Benzene – Naphthacene
Method comparison
Basis-set convergence
Functional dependence

## Slide 95: Method comparison ionization potentials

## Slide 96: Method comparison electron affinities

## Slide 97: G0W0 basis-set convergence
Tested for all molecules
In general linear extrapolation possible especially to the DEF2 results
TZVPP in this test set converged within 0.25 eV
SVP
TZVP
TZVPP
QZVP
cc-pVDZ
cc-pV5Z
cc-pVQZ
cc-pVTZ
Extrapolated results

## Slide 98: Basis set convergence
Deviation from the extrapolated results

## Slide 99: G0W0 Functional dependence
Differences between G0W0 results (Δ) are much smaller than deviations between the respective DFT results
Largest differences for LiH, H2O and hydrocarbons with OH groups

## Slide 100: Open shell systems
Collinear case
  Matrices are spin-diagonal
  Screening comes from both spin channels

## Slide 104: +
http://www.pseudo-dojo.org
ONCVPSP potentials from the Pseudo-Dojo
9.2
0.07
0.02
0.14
0.44
0.18
0.28
0.91
0.36
0.10
1.33
0.95
1.04
1.02
0.24
0.11
0.54
0.41
0.28
0.47
0.29
0.99
1.04
0.05
0.17
0.29
0.72
0.04
0.68
0.44
0.33
Mn. Minimum at Ar
0.05
0.01
0.03
0.04
0.05
0.07
0.47
0.21
0.17
0.21
1.23
0.90
1.25
3.53
11.7
5.31
2.10
1.18
0.85
0.10
1.02
0.79
1.43
1.42
1.68
1.78
2.01
1.22
0.52
1.86
0.37
0.73
2.71
0.68
0.88
1.39
2.45
0.58
0.38

## Slide 105: Table of ONCVPSPs
NC with/without semi-core states
Good log derivative up to 3-5 Ha
Validated with DF, GBRV tests, Phonons
Deltafactor:
1.0 meV (best pseudo for each element, including Mn!)
1.6 meV (all pseudos)
Mn