## Slide 1: Imaging the electrocaloric effect at the nanoscale
Valentin Fonck
Jean Spièce
Charalambos Evangeli
Pascal Gehring

## Slide 2
The electrocaloric effect
Thermodynamics
…
Pandya, S. et al. Phys. Rev. Appl. 7, 034025 (2017).
Iguchi, R. et al. Applied Physics Letters 122, 082903 (2023).

## Slide 3
Motivations
Moya, X., Defay, E., Mathur, N. D. & Hirose, S. MRS Bulletin 43, 291–294 (2018).
Can we build an electrocaloric nanoscale fridge ?
On-chip spot-cooling
Sensor cooling
Individual cell manipulation
Technique |  | COP/COPCarnot
Vapor-Compr. | >20 | 60%
Thermoelectric | 30 | 10%
« Caloric » methods (electro, magneto-, eslasto…) |  | Up to 80%
Technique |  | COP/COPCarnot
Vapor-Compr. | >20 | 
Thermoelectric |  | 10%
« Caloric » methods (electro, magneto-, eslasto…) |  | Up to 80%

## Slide 4
The electrocaloric effect
Direct methods
Indirect methods
Indirect methods
Local methods
Spatially averaged
Pandya, S. et al. Phys. Rev. Appl. 7, 034025 (2017).
Iguchi, R. et al. Applied Physics Letters 122, 082903 (2023).
Limited to >1m resolutions
Requires sample fabrication

## Slide 5
Scanning Electrocaloric Thermometry
Can we apply a local electric field ?
air
Si
Local electric field
Nanoscale thermometry
Scanning electrocaloric thermometry (SeCT)

## Slide 6
Local imaging

## Slide 7
Local imaging
4um
Excitation matters
Frequency matters

## Slide 8
Scanning Electrocaloric Thermometry
hBN
PVDF-TrFE
Control experiment
No response  Not a contact artifact
Polarisable 2D material
Unipolar vs bipolar excitation
Ferroelectric thin film
Writing and writing polarisation
Polarisation dependent ECE response

## Slide 9
Takeaway message
With this technique you can simultaneously :
Image the ECE at the nanometer scale
Separate the Joule response from the ECE
Perform PFM measurement
Write FE domains and image them
It can be performed on any polarisable material (ferro-, para- or dielectric)

## Slide 10
Are you looking for a postdoc ? pascal.gehring@uclouvain.be

## Slide 11
Raman spectroscopy
Liu, L. et al. Atomically Resolving Polymorphs and Crystal Structures of In2Se3. Chem. Mater. 31, 10143–10149 (2019).

## Slide 12
PVDF PFM response

## Slide 13
Approach curve