## Slide 1: Advancing GW
A benchmark set for molecules
High throughput methods for solids
Michiel van Setten

## Slide 2: GW
Density functional theory
  Maps the many particle problem into a single particle problem
  Scalar effective potential Vxc(r)
  Applicable to large systems: > 2000 atoms
  Broadly used across many fields of sciences
  Description of electronic levels (charge transfer), long range interactions, and band gaps not accurate enough
GW-method
  Replace the potential by a self-energy matrix: Vxc(r) → Σ(r,r’,E)
  Becoming increasingly available for bulk solids
  Starts to gain terrain for calculations on molecules
  Significantly improved description of electronic levels (charge transfer), long range interactions, and band gaps
  Complex and expensive calculations

## Slide 3: A benchmark set for molecules
GW100

## Slide 4: Benchmark set for molecules: GW100
Collaboration KIT Karlsruhe, FHI Berlin and Berkeley Lab US DoE
  TURBOMOLE: Gaussian basis sets, spectral representation via Casida
  FHI-Aims: numerical local orbitals, analytic continuation
  BerkeleyGW: plane waves, plasmon pole and real frequency integration
  5 different ways to evaluate the self-energy
Strictly converged all electron reference values for IP and EA

## Slide 5: Hard to converge

## Slide 6: Problems when solving the QPE
x

## Slide 7: Self-Energies

## Slide 8: Some numbers
0.65 eV overestimation by plasmon pole
0.32 eV underestimation at QZVP level for the LUMO
0.12 eV underestimation at QZVP level for the HOMO
0.12 eV error by two pole analytic continuation
0.10 eV error by introducing a 150 eV cutoff on empty states and a 544 eV cutoff on the dielectric matrix
0.05 eV overestimation by RI auxiliary basis functions
0.05 eV error by introducing a 400 eV cutoff on the spectral representation of the response function

## Slide 9: Collaborators
Florian Weigend (KIT Karlsruhe)
Ferdinand Evers (KIT Karlsruhe)
Fabio Caruso (FHI Berlin)
Patrick Rinke (FHI Berlin)
Sahar Sharifhades (Berkeley Lab)
Jeffey Neaton (Berkeley Lab)

## Slide 10: High throughput GW for solids
from a structure without any human intervention to converged GW results ?

## Slide 11: GW in High Throughput
‘additional’ difficulties
  4 step calculation
  N4 scaling
  No ‘safe’ parameter set (converged results for all)
  No ‘safe’ computational settings (ncpu, mem, ..)
DFT babysitting problem

## Slide 12: GW in High Throughput
‘additional’ difficulties
  4 step calculation
  N4 scaling
  No ‘safe’ parameter set (converged results for all)
  No ‘safe’ computational settings (ncpu, mem, ..)
GW babysitting problem

## Slide 13: GW wrapper
Python package that wraps around the ab-initio code
Options
    Vasp / Abinit
    What kind of GW
    (currently fixed) K-point density
    Convergence tolerance
Some list of structures > ‘fully’ converged GW results

## Slide 14: Convergence study
On a low k-point density (2x2x2):
  Set of single parameter ground state convergence studies
  Grid of nbands X encuteps
  For each nbands find converged encuteps
  For the converged encuteps find the converged nbands
  if not found > extend grid and retest
On the final k-point density (500):
  Test if the converged values have comparable derivatives to those calculated in the lower density grid. (in most cases the high density derivatives turn out smaller)
  Post process (create scissor, apply scissor, …)
(ecut, …)

## Slide 16
G-G gap
(eV)

## Slide 17
G-G gap
(eV)

## Slide 18
G-G gap
(eV)

## Slide 19: dielectric matrix cutoff

## Slide 20: @ converged parameters
Test at high KP-density by comparing derivatives
Store results in a database, create scissor operators, … … do some actual physics

## Slide 21: Pseudo Potentials …

## Slide 22: ONCVPSP
Optimized Norm Conserving Vanderbild Pseudo Potentials
  multiple projectors
  multiple gradient constraints
Don Hamann (PRB 88, 085117 (2013))
Package to facilitate PSP generation
Graphical interface
Automatized testing
http://www.pseudo-dojo.org/dojo.html

## Slide 23: Collaborators
Matteo Giantomassi
Geoffroy Hautier
Gian-Marco Rignanese
Jean-Michel Beuken
http://pymatgen.org
AbiPy
https://github.com/gmatteo/abipy

## Slide 24: Band convergence

## Slide 26: independent sub-’Packages’
Error parser / handler for scheduler related job terminations.
Convergence tester
    Determine asymptotic value even for a low number of data points

## Slide 27: Pseudo Dojo
Automatic testing and training of PSPs
Connections to PSP generator codes via an graphical interface.
Flexible tests, automatic PSP improvement

## Slide 28: PseudoDojo current status
Automatic testing with Abinit
  DeltaFactor Elemental Solids
  Energy cutoff convergence of DF for ES
  Energy cutoff convergence of Total Energy for ES
  Lattice parameter FCC and BCC solids
Testing against precalculated All Electron results @ specified parameters

## Slide 29: Pseudo Potentials …

## Slide 30: Energy dependent scissor

## Slide 31: Old stuff

## Slide 32
G-G gap
(eV)

## Slide 33
PAW

## Slide 35
(eV)

## Slide 43
G-G gap
(eV)

## Slide 44
ENCUTGW (eV)
G-G gap
(eV)

## Slide 45
G-G gap
(eV)

## Slide 46
G-G gap
(eV)

## Slide 47
G-G gap
(eV)

## Slide 48
G-G gap
(eV)

## Slide 49
GWSpec
  Systems (list of structures or files)
  Functional
  Code (ABINIT, VASP)
  Precision , kpdens
  Kind of GW
  Mode (input, input with jobfiles, fw)

## Slide 50
Loop over structures
    Add special points
Loop over jobs
    Job (G0W0) > work (specified) > tasks
Create input / job structure / FW workflow

## Slide 51: ‘Kresse set’
Si, GaAs, SiC, CdS, AlP, GaN, ZnO, ZnS, C, BN, MgO, LiF, Ar, Ne
Vasp/abinit
Exciting is also running

## Slide 52
Chart: ENCUTGW 150 - 400 (400 == 1)
 | 0.99711 | 1.0539 | 0.95842 | 0.96772 | 0.98698 | 0.99368 | 0.95981 | 0.99836 | 0.9752 | 0.96874 | 0.97934 | 0.9863 | 0.99786 | 1.0016
 | 1.004 | 1.0209 | 0.98118 | 0.98032 | 0.99642 | 1.0002 | 0.97719 | 0.99782 | 0.98818 | 0.9851 | 0.99336 | 0.99396 | 0.999 | 1.0003
 | 1.0037 | 1.0043 | 0.99233 | 0.9871 | 0.99875 | 1.0009 | 0.98775 | 0.9982 | 0.99485 | 0.99346 | 0.99812 | 0.99799 | 0.9998 | 0.99994
 | 1.0017 | 1 | 0.99708 | 0.99253 | 0.99952 | 1.0004 | 0.99482 | 0.99886 | 0.99782 | 0.99739 | 0.99974 | 0.99935 | 1 | 0.99998

## Slide 53
Chart: NOMEGA 80 - 120 (120 == 1)
 | 1.0951 | 1.007 | 1.0288 | 1.0541 | 1.0278 | 1.0053 | 1.0652 | 1.0152 | 1.0002 | 1.0002 | 1.0004 | 1.0001 | 0.99987 | 0.9997
 | 1.0338 | 1.0016 | 1.0095 | 1.0195 | 1.0105 | 1.0035 | 1.0277 | 1.0051 | 0.99986 | 1.0003 | 1.0003 | 1.0006 | 0.9998 | 1.0005

## Slide 54
Chart: NBANDS *10 - *30 (30 == 1)
 | 0.96819 | 1.1549 | 0.96793 | 0.9767 | 0.9629 | 0.98078 | 0.97065 | 1.0025 | 0.99392 | 0.98051 | 0.97959 | 0.99034 | 0.97958 | 0.99629
 | 0.98363 | 1.121 | 0.98564 | 0.98837 | 0.98073 | 0.99052 | 0.98403 | 1.0034 | 0.99699 | 0.99077 | 0.98905 | 0.99556 | 0.98631 | 0.99775
 | 0.99199 | 1.0186 | 0.99383 | 0.99332 | 0.99045 | 0.99689 | 0.99449 | 0.99896 | 0.99895 | 0.99657 | 0.99553 | 0.99698 | 0.99251 | 0.99862

## Slide 55: Ar
40 : 201 bands 158 eV

## Slide 56: Ar

## Slide 57: LiF
40 : 281 bands 355 eV

## Slide 58: BN
40 : 241 bands 400 eV

## Slide 59: C diamond
40 : 229 bands 416 eV

## Slide 61
Chart: KP_GRID_DENS 500, 1000, 2000 (2000 == 1)
 | 0 | 0.99989 | 0 | 0 | 0.97488 | 0.99065 | 0.98483 | 1.0031 | 1.009 | 0.98177 | 0 | 0 | 0 | 0
 | 0 | 0.99198 | 0 | 0 | 0.97806 | 0.9997 | 1.0018 | 1.0019 | 0.99991 | 0.98274 | 0 | 0 | 0 | 0
 | 0 | 1 | 0 | 0 | 1 | 1 | 1 | 1 | 1 | 1 | 0 | 0 | 0 | 0

## Slide 62: Other sets
P-type TCO’s
Van Schilfgaarde set
  AE data exists
Hautier set ;-)
  Much more balanced
  HSE06 and Tran Blaha data