## Slide 1
Chart: Kov x 105 (m3/m2s)
| PVDF* | PVDF-PDA* | PVDF-PDA-PIL (VEIm Br)* | PVDF-PDA-PIL (VApIm Br) | PVDF-PDA-PIL (VEIm Br)-CA* | PVDF-PDA-PIL (VApIm Br)-GLU-CA
 | 2.5346 | 2.3887 | 1.5496 | 2.6031 | 6.1553 | 7.5723
References
Conclusion
Results and Discussion
Acknowledgements
This work is supported by the Communauté française de Belgique under the context of FRIA scholarship grant; and previously supported by the European Research Council, ERC starting grant.
Context
Methodology
The best IL monomer concentration (0.25 g/mL) and chitosan concentration (2.0 %w/v) was one that yielded smooth, well coated surface.
The best immobilization conditions resulted in optimum crosslinker concentration (1.0% v/v) for the available PIL amino binding group, under a pH condition (pH 9.0) that was optimal for electrostatic binding between the enzyme and PIL coated surface.
[VApIm][Br] that allowed covalent immobilization of CA resulted in up to 300% increased CO2 capture performance relative to pristine PVDF membrane, and is reusable up to 4 times.
Ionic liquid monomer composition
Kamyll Dawn Cocon1, Kimberly Gonçalves Santos, Cristhian Molina-Fernandez2, Patricia Luis1
1 Institute of Mechanics Materials and Civil Engineering, IMAP, Université catholique de Louvain, Belgium
2 Department of Chemical Engineering, Université de Liège, Belgium
kamyll.cocon@uclouvain.be, patricia.luis@uclouvain.be
Polyionic liquid deposited biocatalytic membrane contactor for intensified CO2 capture and conversion into bicarbonate
Gas-phase
CO2
HCO3-
Liquid-phase
CO2 absorption test
CO2 absorption test
Future work
Improve enzyme loading:
Center-radial
Pore2
Dendritic nanoparticles
Intensified CO2 conversion:
Nanobiocatalyst3
Improve eco-friendliness:
Bio-based membranes
The objective is to increase CO2 absorption in a benign, aqueous-based liquid absorbent by improving the overall mass transfer coefficient via: (1) catalyzing CO2 conversion into HCO3- using carbonic anhydrase, (2) supporting the reaction by increasing CO2 concentration near CA by using high-CO2 affinity IL.
PIL deposited biocatalytic membranes significantly increased overall CO2 mass transfer coefficient. PIL synthesized in this work ([VApIm][Br]) showed better performance than in literature ([VEpIm][Br]).
(c)
Imidazolium-based PIL layer preparation
[VApIm][Br] quaternary reaction
1 Molina-Fernández, C. & Luis, P. Immobilization of carbonic anhydrase for CO2 capture and its industrial implementation: A review. J Co2 Util 47, 101475–101475 (2021).
2 Du, X. & Qiao, S. Z. Dendritic Silica Particles with Center-Radial Pore Channels: Promising Platforms for Catalysis and Biomedical Applications. Small 11, 392–413 (2015).
3 Misson, M., Du, X., Jin, B. & Zhang, H. Dendrimer-like nanoparticles based β-galactosidase assembly for enhancing its selectivity toward transgalactosylation. Enzyme Microb Tech 84, 68–77 (2016).
UCLouvain
Absorption conditions:
Gas flow-rate: 0.4 Ln/min (15% CO2, 85% N2)
Liquid flow-rate: 0.6 L/min (0.5 M Na2CO3)
25°C, 1 h
Porous membrane
Polyvinylidenefluoride
Contact 2 h, 25 °C
Rinsing isopropanol
Drying 12h, 25 °C
Surface modification
Dopamine: 2 mg/mL
Amino-functionalized
membrane
- - -
+ + +
A
A
A
A
A
Shaking 24 – 48 h, 25 °C
Wash Ultrapure Water
Enzyme immobilization
Glutaraldehyde: 0.67 – 1.67 %v/v
B
B
B
B
B
Biocatalytic membrane
A
A
A
A
A
N2
UV-polymerization
2 h, N2 rich environment
PIL layer
PIL-deposited membrane
Neutralization
0.1 M Na2CO3, 2 h
Enzyme immobilization
Tris-HCl solution
50 mM,
pH 8.5
Tris-HCl,
50 mM
pH 8.5
Tris-HCl solution
50 mM,
pH 8.5
Enzyme solution
0.5 – 0.8 mg/mL,
pH 6 – 10
Tris-HCl solution
50 mM,
pH 8.5
[VApIm][Br]: 0.1 – 0.35 g/mL
Chitosan: 0.3 – 0.5 %wt/v
2-hydroxy-2-methylpropiophenone (1 %w/w)
IL monomer solution
CO2
CO2
CO2
3-PGA
RuBisCO
CO2
Carbonic
anhydrase
HCO3-
+ RUBP
CO2
CO2
X
+
-
+
-
+
-
+
-
Polyionic liquid
Increase CO2 transfer
+
Problem
Proposal
Solution
PLA
Solvent
Enzyme immobilization
Chart: pH
| 6 | 7.5 | 8 | 9 | 10
 | 0.01803 | 0.031813 | 0.11376 | 0.58821 | 0.30556
Chart: Glutaraldehyde concentration [% v/v]
| 0.67 | 1 | 1.33 | 1.67
 | 0.2362 | 0.58821 | 0.16482 | 0.14358
Chart: Enzyme concentration (mg/mL)
| 0.5 | 0.6 | 0.7 | 0.8
 | 0.46073 | 0.88931 | 1.2179 | 0.51271
Chart: Monomer concentration [g/mL]
| 0.1 | 0.15 | 0.2 | 0.25 | 0.3 | 0.35
0,273320509 0,239342249 0,579320428 0,746923938 0,451356385 0,54736855 | 0.27332 | 0.23934 | 0.57932 | 0.74692 | 0.45136 | 0.54737
Chart: Chitosan concentration [% wt/v]
| 1.5 | 2 | 2.5 | 3
 | 0.34158 | 0.74692 | 0.66311 | 0.33056
Increasing chitosan concentration resulted in decreased enzyme activity, probably due to reduced available amino groups for enzyme binding
Increasing IL monomer concentration resulted in increased viscosity and denser PIL coating
+ 237%
+ 300%
Reference
Chart: Cycle
 | 7.5723 | 7.6751 | 11.0859 | 7.0096
PIL deposited biocatalytic membrane was stable under the conditions studied (4 cycles).
Cycle 0
Cycle 4 (post)
PVDF
PVDF - PDA
0.10 g/mL
0.25 g/mL
0.35 g/mL
1.5 %w/v
2.0 %w/v
3.0 %w/v
Monomer
Chitosan
IL absent
Increasing glutaraldehyde concentration allowed more enzyme to be immobilized up to a point, and then results in lower activity due to stearic hindrance.
Increasing pH allows the enzyme to exhibit negative charge (pI = 5.91) that supports surface binding. At high pH (pH = 10), the enzymes suffers from denaturation
Reusability
Nature-inspired (cyanobacteria)
Liquid
Liquid film
Gas film
Gas
Porous membrane