Supporting Information

Recent advances in the application of CuAAC for the covalent immobilization of homogeneous catalysts, a decade of progress

Antony E. Fernandes,a,* Olivier Riant,b and Alain M. Jonasb

a Certech, Rue Jules Bordet n°45, Zone Industrielle C, 7180 Seneffe, Belgium

b Institute of Condensed Matter and Nanosciences (IMCN), Université catholique de Louvain (UCLouvain), Croix du Sud 1/L7.04.02, 1348 Louvain-la-Neuve, Belgium

| reference | support | Cu source | reducing agent | ligand | solvent | reaction time | T°C | mol% Cu | mol% red | mol% ligand | CuAAC yield |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| M.C. Lukowiak, M. Meise, R. Haag, Synthesis and Application of N-Heterocyclic Carbene–Palladium Ligands with Glycerol Dendrons for the Suzuki–Miyaura Cross-Coupling in Water, Synlett, 25 (2014) 2161-2165. | azide dendrons | CuSO4·5H2O | sodium ascorbate | DIPEA | H2O-MeOH (1:1) | 3-7d | rt | 10 | 20 | 20 | 22-45 |
| A.R. Hajipour, P. Abolfathi, F. Mohammadsaleh, A click strategy for the immobilization of palladium nanoparticles onto silica: efficient and recyclable catalysts for carbon–carbon bond formation under mild reaction conditions, RSC Advances, 6 (2016) 78080-78089. | azide silica | CuSO4·5H2O | sodium ascorbate | no | H2O-MeOH (1:1) | 3 d | rt | na | na | 0 | na |
| A.R. Hajipour, F. Mohammadsaleh, Triazole-Functionalized Silica Supported Palladium(II) Complex: A Novel and Highly Active Heterogeneous Nano-catalyst for C–C Coupling Reactions in Aqueous Media, Catal. Lett., 148 (2018) 1035-1046. | azide silica | Cu2O | no | no | H2O-MeOH (1:1) | 3 d | rt | na | 0 | 0 | na |
| A. Saad, C. Vard, M. Abderrabba, M.M. Chehimi, Triazole/Triazine-Functionalized Mesoporous Silica As a Hybrid Material Support for Palladium Nanocatalyst, Langmuir, 33 (2017) 7137-7146. | azide silica | CuSO4 | sodium ascorbate | no | H2O-iPrOH (1:1) | 24 h | rt | na | na | 0 | na |
| H.-K. Lo, C. Copéret, CO2 Hydrogenation to Formate with Immobilized Ru-Catalysts Based on Hybrid Organo-Silica Mesostructured Materials, ChemCatChem, 11 (2019) 430-434. | azide silica | CuSO4·5H2O | sodium ascorbate | no | DMF | 48 h | rt | 32 | 62 | 0 | na |
| A. Desmecht, T. Steenhaut, F. Pennetreau, S. Hermans, O. Riant, Synthesis and Catalytic Applications of Multi-Walled Carbon Nanotube-Polyamidoamine Dendrimer Hybrids, Chemistry, 24 (2018) 12992-13001. | azide MWNT | CuI | no | PMDETA | DMF | 72 h | rt | 100 | 0 | 100 | na |
| I. Pernik, A. Desmecht, B.A. Messerle, S. Hermans, O. Riant, Dendrimeric and Corresponding Monometallic Iridium(III) Catalysts Bound to Carbon Nanotubes Used in Hydroamination Transformations, Eur. J. Inorg. Chem., 2021 (2021) 3448-3457. | azide PAMAM MWNT | CuI | no | PMDETA | DMF | 72 h | rt | 10 | 0 | 10 | na |
| D. Sheet, A. Bera, Y. Fu, A. Desmecht, O. Riant, S. Hermans, Carbon-Nanotube-Appended PAMAM Dendrimers Bearing Iron(II) alpha-Keto Acid Complexes: Catalytic Non-Heme Oxygenase Models, Chemistry, 25 (2019) 9191-9196. | azide PAMAM MWNT | CuSO4·5H2O | sodium ascorbate | no | MeOH | 48 h | rt | 12 | 32 | 0 | na |
| A.K. Beurer, M. Kirchhof, J.R. Bruckner, W. Frey, A. Baro, M. Dyballa, F. Giesselmann, S. Laschat, Y. Traa, Efficient and Spatially Controlled Functionalization of SBA‐15 and Initial Results in Asymmetric Rh‐Catalyzed 1,2‐Additions under Confinement, ChemCatChem, 13 (2021) 2407-2419. | azide silica | CuSO4·5H2O | sodium ascorbate | no | H2O | 72 h | rt | 150 | 300 | 0 | na |
| Z. Li, L. Rösler, T. Wissel, H. Breitzke, T. Gutmann, G. Buntkowsky, Immobilization of a chiral dirhodium catalyst on SBA-15 via click-chemistry: Application in the asymmetric cyclopropanation of 3-diazooxindole with aryl alkenes, Journal of CO2 Utilization, 52 (2021). | azide silica | CuBr(PPh)3 | no | DIPEA | toluene | 48 h | 40°C | na | 0 | na | na |
| D. Wang, C. Deraedt, L. Salmon, C. Labrugere, L. Etienne, J. Ruiz, D. Astruc, A tris(triazolate) ligand for a highly active and magnetically recoverable palladium catalyst of selective alcohol oxidation using air at atmospheric pressure, Chemistry, 21 (2015) 6501-6510. | azide SiO2 @Fe2O3 NP | CuI | no | DIPEA | DMF-THF (1:1) | 48 h | rt | na | 0 | na | na |
| N. Pentela, P. Murugan, S.N. Jaisankar, D. Samanta, A.B. Mandal, Immobilization of ruthenium benzylidene on thermoresponsive polymer: Methodology and application, J. Organomet. Chem., 778 (2015) 42-46. | azide ethanol | CuSO4·5H2O | sodium ascorbate | no | H2O-EtOH (1:2) | 18 h | rt | 10 | 20 | 0 | 70 |
| J. Izquierdo, M.A. Pericàs, A Recyclable, Immobilized Analogue of Benzotetramisole for Catalytic Enantioselective Domino Michael Addition/Cyclization Reactions in Batch and Flow, ACS Catalysis, 6 (2015) 348-356. | azide PS | CuI | no | DIPEA | THF-DMF (1:1) | 16 h | 40°C | 5 | 0 | 350 | 98 |
| R.M. Neyyappadath, R. Chisholm, M.D. Greenhalgh, C. Rodríguez-Escrich, M.A. Pericàs, G. Hähner, A.D. Smith, Acylative Kinetic Resolution of Alcohols Using a Recyclable Polymer-Supported Isothiourea Catalyst in Batch and Flow, ACS Catalysis, 8 (2018) 1067-1075. | azide PS | CuI | no | DIPEA | THF-DMF (1:1) | 24 h | 40°C | 5 | 0 | 350 | 99 |
| N.R. Guha, R.M. Neyyappadath, M.D. Greenhalgh, R. Chisholm, S.M. Smith, M.L. McEvoy, C.M. Young, C. Rodríguez-Escrich, M.A. Pericàs, G. Hähner, A.D. Smith, Evaluating polymer-supported isothiourea catalysis in industrially-preferable solvents for the acylative kinetic resolution of secondary and tertiary heterocyclic alcohols in batch and flow, Green Chemistry, 20 (2018) 4537-4546. | azide PS | CuI | no | DIPEA | THF-DMF (1:1) | na | 40°C | 5 | 0 | 350 | 100 |
| N.R. Guha, R.M. Neyyappadath, M.D. Greenhalgh, R. Chisholm, S.M. Smith, M.L. McEvoy, C.M. Young, C. Rodríguez-Escrich, M.A. Pericàs, G. Hähner, A.D. Smith, Evaluating polymer-supported isothiourea catalysis in industrially-preferable solvents for the acylative kinetic resolution of secondary and tertiary heterocyclic alcohols in batch and flow, Green Chemistry, 20 (2018) 4537-4546. | azide tentagel | CuI | no | DIPEA | THF-DMF (1:1) | 24 h | 40°C | 5 | 0 | 350 | 88 |
| N.R. Guha, R.M. Neyyappadath, M.D. Greenhalgh, R. Chisholm, S.M. Smith, M.L. McEvoy, C.M. Young, C. Rodríguez-Escrich, M.A. Pericàs, G. Hähner, A.D. Smith, Evaluating polymer-supported isothiourea catalysis in industrially-preferable solvents for the acylative kinetic resolution of secondary and tertiary heterocyclic alcohols in batch and flow, Green Chemistry, 20 (2018) 4537-4546. | azide wang resin | CuI | no | DIPEA | THF-DMF (1:1) | 24 h | 40°C | 5 | 0 | 350 | 80 |
| C. Mendoza, A. de la Croix, P. Riente, L. Llorens, J. de Mendoza, M.A. Pericàs, Reusable shuttles for exchangeable functional cargos: Reversibly assembled, magnetically powered organocatalysts for asymmetric aldol reactions, Tetrahedron, 75 (2019) 130592-130601. | azide SiO2 @Fe2O3 NP | CuSO4·5H2O | sodium ascorbate | no | H2O-tBuOH (1:1) | na | na | na | na | na | 70 |
| R.P. Jumde, A. Di Pietro, A. Manariti, A. Mandoli, New polymer-supported mono- and bis-Cinchona alkaloid derivatives: synthesis and use in asymmetric organocatalyzed reactions, Chem Asian J, 10 (2015) 397-404. | azide PS | CuI | no | DIPEA | CH2Cl2 | 2 d | rt | 5 | 0 | 100 | 9 to 35 |
| R.P. Jumde, A. Mandoli, Long-Lived Polymer-Supported Dimeric Cinchona Alkaloid Organocatalyst in the Asymmetric α-Amination of 2-Oxindoles, ACS Catalysis, 6 (2016) 4281-4285. | azide PS | CuI | no | DIPEA | CH2Cl2 | 3 d | rt | 5 | 0 | 100 | 53 |
| W. Yu, M. Zhou, T. Wang, Z. He, B. Shi, Y. Xu, K. Huang, "Click Chemistry" Mediated Functional Microporous Organic Nanotube Networks for Heterogeneous Catalysis, Org. Lett., 19 (2017) 5776-5779. | azide MONN | CuSO4·5H2O | sodium ascorbate | no | H2O-DMF (1:5) | 3 d | rt | na | na | 0 | na |
| J.S. Schulze, J. Migenda, M. Becker, S.M.M. Schuler, R.C. Wende, P.R. Schreiner, B.M. Smarsly, TEMPO-functionalized mesoporous silica particles as heterogeneous oxidation catalysts in flow, Journal of Materials Chemistry A, 8 (2020) 4107-4117. | azide LiChrospher(r) | CuI | no | DIPEA | toluene | 3 d | 50°C | na | 0 | na | na |
| M.C. Nongbe, A. Abolle, V. Coeffard, F.X. Felpin, Rose Bengal Immobilized on Cellulose Paper for Sustainable Visible-Light Photocatalysis, Chempluschem, 87 (2022) e202200242. | azide cellulose paper | CuSO4 | sodium ascorbate | no | THF | 24 h | 80°C | 10 | 100 | 0 | na |
| M. Sebbat, A. Lazar, C. Laurent, C. Despas, N. Vilà, A. Walcarius, N. McClenaghan, E. Oheix, B. Lebeau, M. Cormier, J.-P. Goddard, Heterogenization of [Ru(bpy)3]Cl2 on Ordered Mesoporous Silica Materials for Photocatalytic Applications, Synlett, 36 (2024) 335-340. | azide silica | CuSO4 | sodium ascorbate | no | H2O-DMF (3:7) | 24 h | rt | na | na | 0 | na |
| P. Kasaplar, E. Ozkal, C. Rodríguez-Escrich, M.A. Pericàs, Enantioselective α-amination of 1,3-dicarbonyl compounds in batch and flow with immobilized thiourea organocatalysts, Green Chemistry, 17 (2015) 3122-3129. | azide PS | TTM.CuCl | no | no | DMF-THF (1:1) | 3 h | 80°C (MW) | na | 0 | 0 | quant. |
| H. Li, M. Pérez-Trujillo, X. Cattoën, R. Pleixats, Recyclable Mesoporous Organosilica Nanoparticles Derived from Proline-Valinol Amides for Asymmetric Organocatalysis, ACS Sustainable Chemistry & Engineering, 7 (2019) 14815-14828. | azide silica | CuI | no | TBTA | THF | 14-16 h | 60-80°C | 20 | 0 | 20 | 100 |
| A.E. Fernandes, O. Riant, A.M. Jonas, K.F. Jensen, One "Click" to controlled bifunctional supported catalysts for the Cu/TEMPO-catalyzed aerobic oxidation of alcohols, RSC Adv., 6 (2016) 36602-36605. | azide silica | CuI | no | Et3N | DMF | o/n | 50°C | 10 | 0 | 500 | 90% |
| A.E. Fernandes, O. Riant, K.F. Jensen, A.M. Jonas, Molecular Engineering of Trifunctional Supported Catalysts for the Aerobic Oxidation of Alcohols, Angew. Chem., Int. Ed., 55 (2016) 11044-11048. | azide silica | CuI | no | Et3N | DMF | 2 d | 55°C | 20 | 0 | 500 | na |
| P. Chandra, A.M. Jonas, A.E. Fernandes, Spatial Coordination of Cooperativity in Silica-Supported Cu/TEMPO/Imidazole Catalytic Triad, ACS Catal., 8 (2018) 6006-6011. | azide silica | CuI | no | Et3N | DMF | 2 d | 55°C | varies | 0 | 500 | 82-96 |
| P. Chandra, A.M. Jonas, A.E. Fernandes, Sequence and Surface Confinement Direct Cooperativity in Catalytic Precision Oligomers, J. Am. Chem. Soc., 140 (2018) 5179-5184. | azide silica | CuI | no | Et3N | DMF | 2 d | 55°C | 120 | 0 | 500 | 71-82 |
| P. Chandra, A.M. Jonas, A.E. Fernandes, Synthesis of discrete catalytic oligomers and their potential in silica-supported cooperative catalysis, RSC Adv., 9 (2019) 14194-14197. | azide silica | CuI | no | Et3N | DMF | 2 d | 55°C | varies | 0 | 500 | 43-89 |
| P. Kasinathan, C. Lang, S. Radhakrishnan, J. Schnee, C. D'Haese, E. Breynaert, J.A. Martens, E.M. Gaigneaux, A.M. Jonas, A.E. Fernandes, "Click" Silica-Supported Sulfonic Acid Catalysts with Variable Acid Strength and Surface Polarity, Chemistry, 25 (2019) 6753-6762. | azide silica | CuSO4 | sodium ascorbate | no | H2O-EtOH (1:2) | o/n | 90°C | 62.5 | 75 | 0 | quant. |
| P. Kasinathan, C. Lang, E.M. Gaigneaux, A.M. Jonas, A.E. Fernandes, A.E. Fernandes, Influence of Site Pairing in Hydrophobic Silica-Supported Sulfonic Acid Bifunctional Catalysts, Langmuir, 36 (2020) 13743-13751. | azide silica | CuSO4 | sodium ascorbate | no | H2O-EtOH (1:2) | o/n | 65°C | 62.5 | 75 | 0 | 84-100 |
| I. García‐Monzón, J. Borges‐González, T. Martín, Solid‐Supported Tetrahydropyran‐Based Hybrid Dipeptide Catalysts for Michael Addition of Aldehydes to Nitrostyrenes, Adv. Synth. Catal., 364 (2022) 2822-2829. | azide PS | CuI | no | DIPEA | DMF-THF (1:1) | 24 h | 35°C | 8 | 0 | 13 | 88 |