Dense packing of molecular hydrogen in a porous hydride and the value of in situ diffraction studies of gas adsorption

Yaroslav Filinchuk

Institute of Condensed Matter and Nanosciences, Université catolique de Louvain

Place L. Pasteur 1, 1348 Louvain-la-Neuve, Belgium

Nanoporous materials have attracted great attention for gas storage, however, high volumetric storage capacity remains still a challenge. We investigate [1] a magnesium borohydride framework with small pores and a unique partially negatively-charged non-flat interior for hydrogen and nitrogen uptake by using neutron powder diffraction, volumetric gas adsorption, inelastic neutron scattering, and first-principles calculations. Hydrogen and nitrogen occupy distinctly different adsorption sites in the pores with very different limiting capacities: 2.33 H2 and 0.66 N2 per Mg(BH4)2. Molecular hydrogen is packed extremely dense with about twice the density of liquid hydrogen (144 g H2/L of pore volume), independently measured by three experimental methods. A penta-dihydrogen cluster is discovered where H2 molecules in one position have rotational freedom whereas in another have a well-defined orientation and a directional interaction with the framework. This study [1] reveals that densely packed hydrogen can be stabilized in small-pore materials at ambient pressures.

Studies of physisorbed hydrogen require the use of neutron powder diffraction. For heavier molecules, in situ X-ray powder diffraction allows to study adsorption thermodynamics and kinetics [2, 3], revealing simultaneously the microscopic origins of guest-host and guest-guest interactions. (Quasi)-equilibrium isotherms and isobars can be built directly from sequential Rietveld refinements, both on adsorption and desorption, thus addressing the hysteresis and kinetics of gas adsorption/desorption. Detailed picture of guest reorganization with an increasing uptake can be obtained.

[1] H. Oh, …, Y. Filinchuk, Small-pore hydridic frameworks store densely packed hydrogen. Nature Chem., 2024, DOI: https://doi.org/10.1038/s41557-024-01443-x

[2] I. Dovgaliuk, V. Dyadkin, M. Vander Donckt, Y. Filinchuk, D. Chernyshov, ACS Appl. Mater. Interfaces 12, 2020, 7710.

[3] I. Dovgaliuk, I. Senkovska, X. Li, V. Dyadkin, Y. Filinchuk, D. Chernyshov, Angew. Chem. Int. Ed., 60, 2021, 5250.