## Slide 1: EMMC 2026 Dimensional accuracy and compression behaviour of copper LPBF lattices Digital Volume Correlation characterization
  Frederik Vanherf
  Joint PhD researcher at KU Leuven and UC Louvain
  AM group KU Leuven and IMAP UC Louvain
  Dr Michel Smet - KU Leuven
  Mohammed Farag - UC Louvain
  Prof Brecht Van Hooreweder - KU Leuven
  Prof Aude Simar - UC Louvain
  frederik.vanherf@kuleuven.be
Notes: Structure:
Introduction: LPBF, lattices, heat transfer devices  problem statement
Mat and methods: discuss setup LMQ – UCS 2 mm samples – (brief) scanning strategies: contour mode, I2O, O2I, H+C – DVC (CT-scan, Deben and Instron compression)
Results:
Show top and side images and PV optim (RD and VF).
RD and VF in function of fo and cm.
Varying beam compensation

## Slide 2: Content
Introduction
Experimental
Results
Conclusions
Adapted contour scanning
Local deviation and porosity distribution
Manufacturing limit
Strain localizations during compression

## Slide 3: Laser Powder Bed Fusion of pure copper
High thermal and electrical conductivity
Low absorption for IR-laser (1080 nm)
Challenging
 Solution
Preheating (300 °C)
Keyhole mode
[ 1 ]
[1] Jadhav, S. D. et al., Laser-based powder bed fusion additive manufacturing of pure copper, Additive Manufacturing, 2021

## Slide 4: Lattices and applications
Energy absorption capabilities [3]
Integration in multi-material components [4]
Lightweighting
Enhance surface area/volume
Locally optimized heat sinks
[2]
[2 ]Kang et al., Green laser powder bed fusion based fabrication and rate-dependent mechanical properties of copper lattices, Materials & Design, 2023
[3] Choong et al, Recent Advances in the 3D Printing of Pure Copper Functional Structures for Thermal Management Devices, In Technologies, 2023
[4] Fraunhofer IGCV, Available online: https://www.igcv.fraunhofer.de/en/research/competences/multi-material.html, 2026
[4]
Notes: Multi-material is long-term goal of my research

## Slide 5: Research goals
Improve dimensional accuracy
Identify manufacturing resolution
Understand compressive behaviour
1
2
3

## Slide 6: Experimental
LPBF of lattices
Laser parameter optimisation
Scanning strategies
Adapted contour mode
Multi-contour (a) vs Contour plus infill (b)
CT-scan
Porosity distribution
Local deviations
Regular quasi-static compression
In-situ CT scans
Manufacturing limit
DVC
(a)
(b)

## Slide 7: Local deviation
0 0.15 0.30
Deviation from CAD model (mm)
Porosity distribution
0.5 mm
0.04 0.37 0.70
Pore distance to surface (mm)
Designed volume fraction: 25 %

## Slide 8: Adapted contour mode
Delay time: 0.6 ms
Scan speed: 1000 mm/s
Notes: Shorter discussion here!

## Slide 9: Adapted contour mode
With scanner delay
Adapted contour mode
Volume fraction: 52.5 %
Volume fraction: 46.5 %
- 6 %
Reducing offset and CAD thickness
Notes: Volume fraction will always be higher than designed

## Slide 10: Manufacturing limit – Point scan BCC
 | High energy | Low energy
UCS 1 mm | 290 ± 21 µm | 201 ± 31 µm
UCS 2 mm | 293 ± 9 µm | 181 ± 15 µm

## Slide 11: Regular quasi-static compression
Designed volume fraction: 14 %
10 x 10 x 10 Unit cells (2 mm)
All with adapted contour mode
Bending-dominated

## Slide 12: Mechanical properties
Baseplate X-position
Baseplate Y-position
Measured VF (designed VF = 14 %)
C+h
I2O
O2I

## Slide 13: Mechanical properties
Gibson-Ashby relations [6]:
Material dependent
Geometry dependent
[7]
[6]Gibson L.J., Ashby M.F. Cellular Solids: Structure and Properties. Cambridge University Press; Cambridge, UK, 1997.
[7] Celik B.B. et al., Tailoring mechanical fatigue behaviour of LPBF-produced metal lattice structures while maintaining high manufacturability, Procedia CIRP, 2024.
Notes: More VF variation than expected

## Slide 14: In-situ CT scans
Incremental DVC

## Slide 15: Incremental DVC
Scanning strategy: contour + hatch
Strain accumulation
Low High
Notes: s5

## Slide 16: Incremental DVC
Scanning strategies comparison
Contour + hatch
Low High
Inner to outer contour
Outer contour to inner
Notes: s5

## Slide 17: Incremental DVC
Scanning strategies at UC scale
Without adapted contour mode
Contour + hatch
Outer contour to inner
Low High
Notes: S2 no cm

## Slide 18: Incremental DVC
Scanning strategy: Point-scan
Min-max – side views
Low High
Notes: S2 no cm

## Slide 19: Conclusions
Dimensional accuracy is challenging for copper because of deep and irregular melt pools
Adapted contour mode can improve irregularities and reduce volume fraction deviation
Point-scan lattices:
identify minimum manufacturing limit
Compressive mechanical properties are unlikely to be affected by the scanning strategy
DVC visualised strain localisations, dominated by strut bending
 scanning strategy does not seem to affect strain behaviour
200 µm
Deviation from CAD
Strain localisations
  Contact me: frederik.vanherf@kuleuven.be

## Slide 20: Laser parameter optimisation
Built Volume Fraction (%)
Relative Density (%)
Backup slides:
Notes: Move to appendix

## Slide 21: Manufacturing limit – Point scan BCC
Notes: Optional

## Slide 22: Segmenting the stress strain curve
Densification strain
Elastic strain
ISO 13314 [5]
Elastic strain
[5] ISO 13314 - Mechanical testing of metals - Ductility testing - Compression test for porous and cellular metals. (n.d.).
Notes: Maybe move to appendix

## Slide 23: Incremental Digital Volume Correlation (DVC)
Large strain: mesh is successively deformed by the displacement field at each step
Iterative solve of a linearized correlation equation to find best displacement vector
[8] Thermo scientific, Reference Guide Avizo 3D, Global DVC approach, 2026
Notes: Move to appendix
Poor texture could be linked to pure copper not having microstructures
When using the DVC global approach, the mesh size results from a trade-off between spatial resolution and measurement uncertainties, often limiting DVC to highly contrasted materials. By adding to the traditional DVC problem (gray-level conservation) a second mechanical problem based on the elastic assumption (equilibrium gap [1]), the displacements that are not mechanically admissible at the scale of the element size (eg. high frequency noise) will be penalized. The new parameter "regularization length" defines the size in which the material is approximated by the linear elastic model and applies the penalization. By properly tuning the regularization length, this procedure can lower the measurement uncertainties and improve the spatial resolution
The resolution of a FE-based DVC problem consists in solving the equation: f(x) = g(x + u(x))
for all position vectors x, where f is the reference image, g the deformed image, and u the sought displacement field. Solving this equation is equivalent to minimizing the correlation residual η=f-g, which should be close to imaging noise. Assuming the conservation of the optical flow between the images, this problem can be linearized and expressed as a matrix inversion problem [5]
with M being the problem matrix, δu the sought increment of displacement at the considered increment, and b the second member (depending of the image gradient of f and of the correlation residual η). M being constant, the resolution of the DVC problem consists in successive update of the second member b after each iteration. The algorithm converges when the displacement increment norm |δu| is smaller than a certain tolerance fixed by the user (usually 1-3 voxels), which means the displacement field u(x) has been correctly measured.
To validate that the algorithm converged to a meaningful value of the displacement field, it is recommended to check the correlation residuals image, η=f-g. The results are deemed trustworthy when the standard deviation of the residuals is limited to the image noise. A non-uniform residual image or a pack of high residuals in the residual histogram indicate that the solution could be improved. Residual maps are presented in the tutorial associated with this module.

## Slide 24: Incremental DVC
Scanning strategy: contour + hatch
Constant range – 3D
Min-max – side view
Low High
Notes: s5

## Slide 25: Incremental DVC
Scanning strategy: Inner contour to outer
Constant range – 3D
Min-max – side view
Low High
Notes: s6

## Slide 26: Incremental DVC
Scanning strategy: outer contour to inner
Low High
Notes: s4

## Slide 27: Incremental DVC
Scanning strategy: without adapted contour mode
Constant range – 3D
Min-max – side view
Low High
Notes: S2 no cm