## Slide 1
Symposium on Schottky Barrier MOS 2024 "The Schottky barrier transistor for neuromorphic applications"
Low-frequency Noise in Polysilicon Source-Gated Transistors
Surrey, 19th September, 2024
Qi Chen1, Valeriya Kilchytska1, Léopold Van Brandt1, Eva Bestelink2, Radu A. Sporea2, Denis Flandre1
1 ICTEAM, UCLouvain, Louvain-la-Neuve 1348, Belgium
2ATI, University of Surrey, Guildford, United Kingdom

## Slide 2
Low-frequency Noise in Polysilicon Source-Gated Thin-Film Transistor
2
J. M. Shannon et al., IEEE Electron Device Lett., 2003.
Advantages
Low saturation voltage
High intrinsic gain
Reduced short-channel effects
Polysilicon Source-gated Transistors (SGT)
Applications
Amplifiers
Drive circuit for displays
Trade-off
Lower current output for the same gate bias and device dimensions due to the Schottky barrier
Why polysilicon?
Balanced cost and electrical characteristics for thin-film large-area circuit applications
Radu A. Sporea et al., IEEE Trans. Electron Devices, 2010

## Slide 3
Low-frequency Noise (LFN) in conventional transistors
McWhorter model (Carrier Number Fluctuation (CNF) model)
Low-frequency Noise in Polysilicon Source-Gated Thin-Film Transistor
Angeliki Tataridou, PhD Dissertation, 2022.
Hooge model (Carrier Mobility Fluctuation (CMF) model)
Low-frequency noise models
3
G. Ghibaudo et al., Microelectron. Reliab., 2002
with
Trap density
Hooge parameter
Physical origin of low-frequency noise traps
Notes: As the downsizing of the geometrical dimensions, Low Frequency Noise has become an important concern for nanoscale transistors.

## Slide 4
Objective and Outline
TCAD simulation and DC measurements
LFN in thin-film transistor (TFT) configuration
LFN in SGT configuration
Conclusions and perspectives
Low-frequency Noise in Polysilicon Source-Gated Thin-Film Transistor
Towards a better understanding of the behavior of low-frequency noise in polysilicon SGT
4
LFN in subthreshold region
LFN in above-threshold region

## Slide 5
Low-frequency Noise in Polysilicon Source-Gated Thin-Film Transistor
1.1. TCAD Simulations
Parameter | Value
Schottky barrier height | 0.35 eV
Polysilicon Mobility | 20 cm·V-1s-1
Polysilicon Permittivity | 11.7
Fixed charge density Qf | 4×1011 cm-2
Acceptor defect density Dit | 1×1012 cm-3
Key parameters used in simulations
Schematic simulated device structure
OhmicDrain
Insulator
Schottky Source with field plate
Gate
Insulator
N-type Polysilicon
5
Doping Dose = 0.5 ×1012 cm-2
VGS ranges from 0 to 20 V, 5V per step
Doping Dose = 0.5 ×1012 cm-2
Simulated IV characteristics
Ich
Ibarrier

## Slide 6
Low-frequency Noise in Polysilicon Source-Gated Thin-Film Transistor
1.1. TCAD Simulations
Transfer and (gm/ID)2 curves at different doping concentrations
6
Decreased doping concentration
SS model for accumulation-mode
device
Decreased doping concentration
VGS –VT = -6 V
VGS –VT = -4 V
VGS –VT = -2 V
VGS –VT = 0 V
VGS –VT = 2 V
Log (Current Density) (A/cm2)
0
3
2
1
4
Variation of current densities
Source Region
Channel
Source Region
Channel
1e17 cm-3
2e17 cm-3
Notes: Short expression

## Slide 7
Low-frequency Noise in Polysilicon Source-Gated Thin-Film Transistor
1.2. Device structure
Schematic of the measured device and measurement configurations
7
Bulk doping dose: 0.5 ×1012 cm-2 & 1.5 ×1012 cm-2
Radu A. Sporea et al., IEEE Trans. Electron Devices, 2010
Gate
Insulator
field plate
Insulator
N-type Polysilicon
120 nm
40 nm
300 nm
Channel
Length
Source
Length
Schottky
Contact
Ohmic
Contact
Source
Drain
Source
Drain
SGT configuration
TFT configuration

## Slide 8
Doping Dose = 0.5 ×1012 cm-2
Transfer curves of SGT and TFT configurations
Low-frequency Noise in Polysilicon Source-Gated Thin-Film Transistor
1.2. IV measurements
On-state current increases by two orders of magnitude in TFT configuration
8
Output curves of SGT and TFT
VGS ranges from 20 to 0 V, -4V per step
Typical SGT output curves with smaller saturation voltages and lower output conductance compared to the TFT configuration
Source Length = 4 um Channel Length = 4 um
VGS ranges from 20 to 0 V, -4V per step
measurement bias points @ VD = 5 V
Notes: Extracted mobility μ = 53 cm·V-1s-1 SGT SS = 0.8 V/dec TFT SS = 1.1 V/dec
The bevaior off-state and subthreshold region is dominated by the channel like in the FET. The negative bias stress normally yields a negative threshold voltage shift of the thin film transistors due to the additional positive charges trapped in the gate dielectrics or at channel/gate insulator interface.

## Slide 9
Low-frequency Noise in Polysilicon Source-Gated Thin-Film Transistor
2. LFN in TFT configuration
The LFN noise behavior are confirmed with the PSD approximately proportional to 1/f
9
Power spectral density (PSD) SId under different doping and fixed current in TFT configuration
Doping Dose = 0.5 ×1012 cm-2
Doping Dose = 1.5 ×1012 cm-2
f -1
VD = 5 V
VD = 5 V
f -1
PSD increases with gate voltage in
subthreshold region
f -1
VD = 5 V
Source Length = 4 um Channel Length = 4 um

## Slide 10
Low-frequency Noise in Polysilicon Source-Gated Thin-Film Transistor
2. LFN in TFT configuration
PSD varies as the reciprocal of ID indicating that the noise in subthreshold region originates from
carrier mobility fluctuation, as in previous reported polysilicon transistors.
ID-1
ID-1
10
Normalized Sid versus ID of TFT configuration
Carrier Mobility Fluctuation (CMF) model
G. Ghibaudo et al., Microelectron. Reliab., 2002
A. Mercha, et al., Journal of Applied Physics, 2001

## Slide 11
Low-frequency Noise in Polysilicon Source-Gated Thin-Film Transistor
3.1 LFN in the subthreshold region of SGT configuration
The LFN noise behavior are confirmed with the PSD approximately proportional to 1/f
11
Power spectral density (PSD) SId in the subthreshold region of SGT configuration without BF2 implant
Doping Dose = 0.5 ×1012 cm-2
Doping Dose = 1.5 ×1012 cm-2
f -1
VD = 5 V
VD = 5 V
f -1
PSD increases with gate voltage in
subthreshold region
Source Length = 4 um Channel Length = 4 um

## Slide 12
Low-frequency Noise in Polysilicon Source-Gated Thin-Film Transistor
3.1. LFN in the subthreshold region of SGT configuration
The normalized PSD at high ID are proportional to (gm/ID)2, indicating the domination of CNF model
VD = 5 V
12
Normalized Sid and (gm/ID)2 versus ID
Carrier Number Fluctuation (CNF) model
ID-1
The normalized PSD at low ID are proportional to ID-1, indicating the domination of CMF model
Notes: Nt ~ 2.46 × 1019 eV/cm3

## Slide 13
13
3.2. LFN in the above-threshold region of SGT configuration
VGS = 0 V
VGS = -5 V
VGS = 5 V
VGS = 10 V
1/f
VGS = 0 V
VDS ranging from 0.1 to 15 V
VTH ≈ -3.6 V
Low-frequency Noise in Polysilicon Source-Gated Thin-Film Transistor
Without BF2 implant
Source Length = 2 um
Channel Length = 10 um
measurement bias points @ VGS = 0 V
Linear
Saturation
f = 10 Hz
Notes: PSD lower than the case with BF2 implant due to less defects induced by implant

## Slide 14
f = 10 Hz
Low-frequency Noise in Polysilicon Source-Gated Thin-Film Transistor
14
3.3. LFN in the above-threshold region of SGT configuration
VGS increases from -2 to 10 V, 2 V per step
VTH ≈ -2.6 V
VDS ranging from 0.1 to 15 V
Linear
Saturation
Source Length = 2 um
VGS = 0 V
1/f
Channel Length = 10 um
With BF2 implant
measurement bias points @ VGS = 0 V

## Slide 15
3.3. LFN model for Schottky barrier transistors
Low-frequency Noise in Polysilicon Source-Gated Thin-Film Transistor
15
with and
Nicolas Clément et al., IEEE Trans. Electron Devices, 2012
A LFN model for Schottky diodes:
What are different for SGTs:
ηVd
In saturation region
PSD no longer depends on the drain voltage, but on the gate voltage in the saturation region!
CMF model

## Slide 16
Low-frequency Noise in Polysilicon Source-Gated Thin-Film Transistor
16
3.3. Dependence of LFN on gate voltage
The normalized PSD as a function of gate voltage VGS
PSD in the saturation region decreases less with gate voltage than that in the linear region
No significant variation of PSD between SGT-saturation and FET-saturation
LFN has negligible dependence on VDS at low VGS
Source Length = 2 um
Channel Length = 10 um
With BF2 implant
f = 10 Hz

## Slide 17
Low-frequency Noise in Polysilicon Source-Gated Thin-Film Transistor
17
3.4. Dependence of LFN on source length
Dependence of polysilicon SGT LFN on source length
PSD decreases with increasing source length
PSD in the saturation region decreases more than that in the linear region ？
VGS = 3 V
Channel length = 10 um
f = 10 Hz
With BF2 implant

## Slide 18
Low-frequency Noise in Polysilicon Source-Gated Thin-Film Transistor
18
3.5. Dependence of LFN on temperature
T = 30 ℃
T = 50 ℃
VGS ranging from 0 to 5 V
VGS ranging from 0 to 5 V
VGS ranging from 0 to 5 V
VDS ranging from 0.1 to 15 V
VDS ranging from 0.1 to 15 V
VDS ranging from 0.1 to 15 V
T = 70 ℃

## Slide 19
Low-frequency Noise in Polysilicon Source-Gated Thin-Film Transistor
19
3.5 Dependence of LFN on temperature
T increases from 30, 50 to 70 ℃
Different normalized PSD as functions of VDS
f = 10 Hz
VGS = 5 V
PSD decreases with increased temperature

## Slide 20
Low-frequency Noise in Polysilicon Source-Gated Thin-Film Transistor
4. Conclusions and perspectives
The variation of buried channel position with gate voltages in high doping case causes a second plateau in the (gm/ID)2
The LFN has a dependence on VDS in linear region
For saturation region, VGS dependence dominates the LFN
No evident difference of LFN between the SGT-saturation region and the FET-saturation region
20
Configuration | LFN Model
TFT | CMF
SGT | CMF for low ID in subthreshold region
 | CNF for high ID in subthreshold region
LFN of polysilicon SGT in subthreshold region
LFN of polysilicon SGT in above-threshold region
Understanding of the physical LFN behavior and modification of LFN model for on-going work of SGT

## Slide 21
Thank you !
Symposium on Schottky Barrier MOS 2024 "The Schottky barrier transistor for neuromorphic applications"
21