Back-gate bias effect on FDSOI MOSFET RF Figures of Merits and Parasitic Elements

B. Kazemi Esfeh1, V. Kilchytska1, B. Parvais2, N. Planes3, M. Haond3, D. Flandre1 and J.-P. Raskin1

1ICTEAM, Université catholique de Louvain, 1348 Louvain-la-Neuve, Belgium

Email: Babak.kazemiesfeh@uclouvain.be, Tel: (+32) 10478386

2Imec, IMEC, Kapeldreef 75, 3001 Leuven, Belgium

3ST, ST-Microelectronics, 850 rue J. Monnet, 38926 Crolles, France

Abstract—This work demonstrates that the back-gate terminal of a 28nm FDSOI MOSFET can be used up to several tens of GHz for signal processing. Furthermore, the dependence of the main RF figures-of-merit on the back gate bias are experimentally extracted using a 3-port characterization in the frequency range of 10 MHz – 26.5 GHz. We propose a small-signal equivalent circuit constructed based on 3-port measurements allowing for more complete extraction of parasitic elements comparing to the 2-ports one. The effect of back-gate bias on cut-off frequencies is demonstrated and explained in terms of its influence on the relevant parasitic elements.

Keywords-cut-off frequencies; FDSOI; 3-port S-parameters;

# Introduction

FDSOI transistors are widely recognized as a promising candidate to continue downscaling beyond the 28 nm-node for low power and mixed-signal CMOS applications ‎[1]. This technology presents key advantages:  Lower variability by using undoped channel ‎[2] and better electrostatic control ‎[3] are amongst the most important improved DC parameters. Moreover, this technology has shown promising RF performances with high current cut-off frequency (fT) and maximum oscillation frequency (fmax) ‎[4]-[5]. One of the most interesting features of this technology is the possibility of back-gate control schemes thanks to ultra-thin buried oxide (BOX) combined with a highly-doped layer underneath the BOX, so called ground-plane (GP), allowing for further improvement of both static and dynamic behaviors of the device ‎[6]. In this work, a 3-ports configuration of FDSOI nMOSFET is employed for extracting the parasitic elements based on an extended small-signal equivalent circuit. The effect of back-gate bias on RF Figures of Merit (FoM) for both front and back gates is investigated and discussed through small-signal equivalent circuit elements.

# Device and measurement setup description

The studied FDSOI nMOSFET is fabricated in the 28 nm FDSOI platform of ST-Microelectronics ‎[7]. Si body, BOX and equivalent gate oxide thickness are 7 nm, 25 nm and 1.3 nm respectively. The channel is rotated by 45° from the <100> plane. The multi-finger device with 40 parallel fingers, 30 nm of length and 1 µm of width each is designed and embedded in coplanar waveguide access pads for RF characterization. The FDSOI nMOSFET has common source configuration that provides the possibility of 3-port measurement in which the front-gate, drain and the back-gate are referred to RF port1, 2 and 3 respectively. Fig. 1a illustrates the simplified cross section: the device layout features a particular access to the back-gate, including a heavily doped n-type GP located below the BOX and an n-well which provides a natural substrate insulation between the devices (so called flip-well architecture ‎[8]). The schematic of the fabricated double-gate nMOSFET is shown in Fig.1b.

(a)

BG

S

S

G

D

S

S

S

S

Short

Open

UTBB

(b)

Fig. 1. (a) Simplified cross section, and (b) the schematic of battery of nMOSFET with open and short de-embedding structures.

“Open” and “short” de-embedding structures are implemented thus allowing for withdrawal of the effects of interconnections on extrinsic capacitances and series resistances. A 4-port Agilent PNAX VNA accompanied with a DC semiconductor-parameter analyzer (HP 4145) are applied to perform the on-wafer 3-port S-parameters measurement up to 26.5 GHz using ground-signal-ground (GSG) pattern infinity probes.

# 3-port RF FOMs extraction

MOSFET RF performance is evaluated by two major FoM, i.e. fT and fmax. By definition, fmax is the frequency at which the (unilateral) power gain is equal to unity (0 dB) and fT is the unity current gain frequency at which the short circuit current gain (h21) becomes unity (0 dB). fT and fmax are extracted from the measured S-parameters extrapolating h21 and unilateral power gain, U, to 0 dB. Similarly to the methodology reported in [9] for 4-port extraction, in case of 3-port S-parameters measurements where port1, port2 and port3 are defined as the front gate, drain and back gate, respectively, h21 and h23 are defined as:

h21=Y21Y33-Y23Y31Y11Y33-Y31Y13    				 (1)

h23=Y23Y11-Y21Y13Y33Y11-Y13Y31    				 (2)

from which cut-off frequency for front-gate (fT) and back-gate (fTbg) can be directly extracted. The unilateral power gain for front gate (U) and back gate (Ubg) are calculated from 3-port Y-parameters as:

U=14∙|Y21-Y12|2ReY11ReY22-ReY21ReY12 			  (3)

Ubg=14∙|Y23-Y32|2ReY33ReY22-ReY23ReY32		  (4)

from which the maximum oscillation frequency for front gate (fmax) and back gate (fmaxbg) are extracted.

Fig. 2 shows the fT and fmax related to the front-gate as a function of Vgs for Vds = 1 V and back-gate biases, Vbg = 0, 1.8 and 3.0 V. As can be seen in Fig. 2a and b, at Vbg = 0 V, the maximum fT and fmax for 30 nm-long device is as high as ~355 GHz. From Fig. 2a and b, it can be seen that application of a positive Vbg interestingly shifts the maximum cut-off frequencies to a lower Vg, however, with slightly decreased peak values. The consequence of the back-gate biasing is firstly, the possibility to get the fT and fmax peak values at lower Vg, as expected, (due to threshold voltage shift with Vbg) and secondly, flatter fT and fmax versus Vg curves, i.e. wider Vg range with maximum values of fT and fmax.

(a)

| Front-gate |  |  |  |  |  |  | Back-gate |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| (Ω) | (Ω) | (mS) | (mS) | (fF) | (fF) | (fF) | (mS) | (fF) | (fF) | (fF) | (fF) | (Ω) |  |
| Rg | Rsd | gmi | gds | Cgstot | Cgdtot | Cdstot | gmbgi | Cbgstot | Cbgdtot | Cbggtot | CWSub | RWell |  |
| 11 | 5 | 50 | 3.8 | 15 | 9 | 21 | 4 | 17 | 2.8 | 1.7 | 11.4 | 30 |  |
| Front-gate |  |  |  |  |  |  | Back-gate |  |  |  |  |  |  |
| (Ω) | (Ω) | (mS) | (mS) | (fF) | (fF) | (fF) | (mS) | (fF) | (fF) | (fF) | (fF) | (Ω) |  |
| Rg | Rsd | gmi | gds | Cgstot | Cgdtot | Cdstot | gmbgi | Cbgstot | Cbgdtot | Cbggtot | CWSub | RWell |  |
| 11 | 5 | 50 | 3.8 | 15 | 9 | 21 | 4 | 17 | 2.8 | 1.7 | 11.4 | 30 |  |

(a)

(b)

Fig. 2. Front-gate (a) fT for Vds = 0.6 and 1 V and (b) fmax for Vds = 1 V as a function of Vg for various Vbg.

Fig. 2a includes results for Vd = 0.6 V. One can see that even at such a low Vd, the device features rather high fT ~280 GHz in a maximum, which is, moreover, stable w.r.t. Vbg (inset in Fig. 2a). Considering low voltage and power applications (< 0.6 V), one can get fT of 280 GHz at Vd = 0.6 V as high as fT for Vd = 1V by Vbg tuning (example is indicated by arrow in Fig. 2a).

(a)

(b)

Fig. 3. Back-gate (a) fTbg and (b) fmaxbg versus Vg for Vbg = 0 and 3 V.

Plots of RF FoMs related to the back-gate transistor fTbg and fmaxbg are illustrated in Fig. 3a and b versus Vgs showing the double gate behavior of FDSOI transistor. From Fig. 3, it can be observed that a maximum fTbg of 55 GHz – 70 GHz and a maximum fmaxbg of 24 GHz – 27 GHz depending on the bias are achieved. The RF FoMs behavior under different Vbg is discussed below in terms of small-signal equivalent circuit and parasitic elements.

# Model and extraction

Based on a 3-port model of FDSOI MOSFET shown in Fig. 1, its small-signal equivalent circuit including both intrinsic and extrinsic components is proposed in Fig. 4. By applying different bias conditions, all elements can be extracted (Table I). Clear advantage of 3-port w.r.t. 2-port measurement [4] is the possibility of more complete extraction of parasitic elements such as e.g. well resistance (RWell), total back-gate capacitance (Cbgtot), etc.

Fig. 4. Complete small-signal equivalent circuit of the 3-port FDSOI MOSFET in saturation including the sum of intrinsic (‘i’) and extrinsic (‘e’) elements denoted by ‘tot’.

Lower gmbgi comparing to gmi (Table I) (due to thicker BOX w.r.t. gate oxide) results, indeed, in a lower fTbg comparing to fT (Fig. 2a and 3a) (see Eq.5). As reported in ‎[9], back-gate resistance (Rbge), the main reason of fmaxbg drop (Eq. 6), is mainly related to the parasitic back-gate network and its value is essentially given by the well. Therefore, fmaxbg is much lower than fmax (Fig. 2b and 3b) due to 3x higher Rbg (RWell) w.r.t Rg (Table I). The reduction of fT and fmax with an increase of Vbg for Vd = 1 V case (Fig. 2) can be explained by the gm (both ‘i’ and “e”) decrease and channel conductance (gds) increase (Table I). Since fmax is dependent on both fT and gds (Eq. 6), the degradation effect on fmax is more pronounced. As shown in Fig. 3a, an increase of Vbg from 0 to 3 V, results in increase of fTbg which is supposed to be mainly due to Cbgtot decrease with Vbg increase (Table I). However, fmaxbg decreases with Vbg increase that could be explained by increasing of gds dominating over the Cbgtot and gmbgi improvement.

Extracted front- and back-gate elements in saturation (Vds = 1 V) and maximum gmi when Vbg = 0 v and 3 V.

| Vbg=3 V |  |  | Vbg=0 V Front-gate |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| (mS) | (mS) | (mS) | (Ω) | (Ω) |  | (mS) |  | (mS) |  | (mS) | (fF) |
| gmi | gme | gds | Rg | Rsd |  | gmi |  | gme |  | gds | Cgtot |
| 58 | 48 | 7.1 | 11 | 5 |  | 60.5 |  | 50.5 |  | 4.5 | 25.7 |
| Vbg=3 V |  |  | Vbg=0 V Back-gate |  |  |  |  |  |  |  |  |
| (mS) | (mS) | (fF) | (fF) |  | (mS) |  | (mS) |  | (Ω) |
| gmbgi | gmbge | Cbgtot | Cbgtot |  | gmbgi |  | gmbge |  | RWell |
| 5 | 3.7 | 15 | 22 |  | 4.8 |  | 4.1 |  | 30 |

fT≈gm2πCgtot					(5)

fmax≈fT2.Rs+Rggds+2πfTRgCgd			(6)

# Conclusion

Effect of back-gate bias on RF FoM of front- and back-gate FDSOI MOSFET is studied based on the 3-port measurements. Back-gate bias application shifts and flattens fT, Fmax versus Vg curves thus giving more flexibility to the designers for the choice of DC points where maximum fT and fmax is achievable. In low-Vg range (<0.5 V), back-gate bias tuning allows fT in low-Vd case to outperform fT in high-Vd case. An equivalent small-signal circuit including back-gate network was reconstructed and main parasitic elements of FDSOI devices were assessed. The effect of back-gate bias on RF FoM was explained through its effect on relevant parasitic small-signal equivalent elements.

##### Acknowledgment

The work was partially funded by Eniac “Places2Be” and Ecsel “Waytogofast” projects.

##### References

International Technology Roadmap for Semiconductor (ITRS), 2011 Edition. <http://www.itrs.com>.

Nobuyuki Sugii et al., “Comprehensive study on vth variability in silicon on Thin BOX (SOTB) CMOS with small random-dopant fluctuation: Finding a way to further reduce variation,” 2008 IEEE International Electron Devices Meeting, San Francisco, CA, 2008, pp. 1-4.

T. Skotnicki et al., “Innovative Materials, Devices, and CMOS Technologies for Low-Power Mobile Multimedia,” in IEEE Transactions on Electron Devices, vol. 55, no. 1, pp. 96-130, Jan. 2008.

B. Kazemi Esfeh, V. Kilchytska, V. Barral, N. Planes, M. Haond, D. Flandre and J. -P. Raskin, “Assessment of 28 nm UTBB FD-SOI Technology Platform for RF Applications: Figures of Merit and Effect of Parasitic Elements,” Solid-State Electronics, vol. 117, pp. 130-137, 2016.

S. Shopov and S. P. Voinigescu, “Characterization of the High Frequency Performance of 28-nm UTBB FDSOI MOSFETs as a Function of Backgate Bias,” 2014 IEEE Compound Semiconductor Integrated Circuit Symposium (CSICS), La Jolla, CA, 2014, pp. 1-4.

Q. Liu et al., “Impact of back bias on ultra-thin body and BOX (UTBB) devices,” 2011 Symposium on VLSI Technology - Digest of Technical Papers, Honolulu, HI, 2011, pp. 160-161.

N. Planes et al., “28nm FDSOI technology platform for high-speed low-voltage digital applications,” 2012 Symposium on VLSI Technology (VLSIT), Honolulu, HI, 2012, pp. 133-134.

J.-P. Noel, O. Thomas, M.-A. Jaud, C. Fenouillet-Beranger, P. Rivallin, P. Scheiblin, T. Poiroux, F. Boeuf, F. Andrieu, O. Weber, O. Faynot and A. Amara, “UT2B-FDSOI Device Architecture Dedicated to Low Power Design Techniques,” ESSDERC 2010, pp. 210-213.

J. C. Barbé, L. Lucci, A. Siligaris, P. Vincent and O. Faynot, “4-port RF performance assessment and compact modeling of UTBB-FDSOI transistors,” 2015 IEEE Radio Frequency Integrated Circuits Symposium (RFIC), Phoenix, AZ, 2015, pp. 355-358.